## Slide 1
Yuanbing Mao, Ph.D. Multifunctional Applications of Oxides (MAO) Laboratory
Department of Chemistry
Illinois Institute of Technology
May 14, 2020
1 PM Eastern
Luminescent Nanoparticles of Metal Oxides

## Slide 2: This Webinar Is Hosted By
ATE Central acts as an information Hub for the National Science Foundation ATE Grantee Community
atecentral.net/webinars

## Slide 3: This Webinar Is Brought To You By

## Slide 4
Mike
Lesiecki, host
Introductions: Host and Moderators
Trevor Thornton
Professor
Arizona State University
Atilla Ozgur Cakmak
Assistant Professor
Penn State University
NACK Network
Notes: I’m Mike Lesiecki, with Luka Partners. I’ll be the moderator for the webinar today and I also serve on EvaluATE’s community college liaison panel. Lori Wingate will is the main presenter for the webinar. She is director of EvaluATE, which is located at The Evaluation Center at Western Michigan University.

## Slide 5: Introductions
Presenter
Yuanbing Mao, PhD
Professor and Chair
Department of Chemistry
Illinois Tech

## Slide 6
Acknowledgements (2010 – present)
Visiting Scholars:
Dr. H Liu
Dr. W. Luo
Dr. L. Mao
Dr. L. Yi
Dr. L. Tian
Postdoctoral Fellows:
Dr. J. Ahmed
Dr. S. Gupta (Fulbright)
Dr. M. Pokhrel
Dr. B. Srivastava
Dr. Y. Tian
Dr. J. Zhao
Undergraduates (> 60):
Mr. A. Altecor (Rice U  DuPont)
Mr. A. Arguelles (TAMU)
Ms. J. Bravo (Iowa State U)
Ms. Y. Cantu (Texas State U)
Mr. H. Chirino (UTRGV)
Ms. D. Concha (Baylor C)
Mr. K. Diab (UT Medical School)
Ms. E. Garcia (Great Mills Co.)
Ms. B. Gonzalez (UTRGV)
Ms. A. Lopez (UTRGV)
Ms. Q. Lu (Sharyland ISD)
Mr. L. Lu (UTRGV)
Ms. D. Owens (McAllen ISD)
Ms. M. Palacios (UT Medical School)
Mr. J. Shaikh (Medical School)
Ms. M. Valdez (UTRGV)
Mr. E. Villarreal (Rice U, NSF GF)
Mr. K. Wahid (UT Medical School)
etc.
High School Interns (> 18):
P. Aguirre (UTRGV), A. Flores, M. Gorena, S. Maldonado, A. Ramos, A. Rocha, M. Trejo, H. De Santiago (UTRGV), M. Valdez (UTRGV), C. Waters (TAMU), etc.
Graduate Students:
Mr. S. Alaparthi (WV State U)
Ms. P. Kukkapalli (Guardian Drug Co.)
Mr. Q. Li (TAMU  Purdue U)
Ms. W. Lin (Iowa State U)
Ms. X. Sun (TAMU  Purdue U)
Ms. Christina Figueroa (UTRGV)
Mr. M. Hakim Marjuban (UTRGV)
Mr. O. Oriretan (UTRGV)
Ms. M. Penilla (UTRGV)
Mr. J. Zuniga (Moltex Energy, Canada)
Ms. F. Jahanbazi (Current)
Mr. T. Abeywickrama (Current)
Jan. 18, 2019

## Slide 7
$$:
Acknowledgements (2010 – present)
Collaborators:
Dr. S. Banerjee (TAMU)
Dr. J. Borchers (NIST)
Dr. A. Burger (Fisk U)
Dr. X. Chen (Columbia U)
Dr. J. Dorman (LSU)
Dr. Z. Feng (OSU)
Dr. B. Guiton (UKentucky)
Dr. E. Kelley (NIST)
Dr. K. Lozano (UTRGV)
Dr. K. Martirosyan (UTRGV)
Dr. J. Neuefeind (ORNL)
Dr. A. Puretzky (ORNL)
Dr. L. Sun (UConn)
Dr. M. Therien (Duke U)
Dr. D. Wall (WSU)
IIT Startup
UTPA Startup UTPA FRC
UTPA FDFP
UTPA URI
UTRGV FRC

## Slide 8
Outline
Intro
PL and RL
PerL
UC
Summary

## Slide 9
Metal Oxides
Chemical compounds containing at least one oxygen atom as well as at least one metallic element.
Cr3+:Al2O3
https://www.sigmaaldrich.com/materials-science/material-science-products.html?TablePage=112202335

## Slide 10
Luminescence
A light emission which represents an excess over the thermal radiation and lasts for a time exceeding the period of electromagnetic oscillation.
A form of cold-body radiation vs. incandescent light.
Loses correlation between phases of absorbed and emitted light vs. reflected and stray light.
https://www.phenix.bnl.gov/phenix/WWW/publish/barish/publish/wasiko/Copy/Solar/Luminescence%20and%20Fluorescence%20Spectroscopy.htm
Brief history:
‘Afterglow’ traced back to ~1000 years
First observed fluorescence from quinine by Sir J.F.W. Herschel in 1845
G.G. Stokes coined the term ‘fluorescence’ in 1853
E. Wiedemann used the term ‘luminescence’ in 1888
Basic principles of fluorescence were mostly developed during the 1020’s and 1930’s:
Excited state lifetime (Gaviola)
Quantum yield (Wavilov)
Polarization of fluorescence (Weigert, F. Perrin)
Jablonski diagram (A. Jablonski)
Fluorescence resonance energy transfer by T. Förster in the 1950’s
Upconversion by F. Auzel in the 1960’s

## Slide 11
Luminescence
Jablonski diagram and spectra showing the fundamental photophysical processes in organic molecules:
Absorption of a photon: S0  S1,S2
Internal conversion: S2  S1 (non-radiative)
Fluorescence: S1  S0
Intersystem crossing: S1  T1
Phosphorescence: T1  S0
https://www.lambertinstruments.com/technologies-1/2014/12/4/frequency-domain-flim-basic-equations

## Slide 12
Luminescence
Cr3+:Al2O3
Luminescence Characterization:
Excitation spectroscopy
Emission spectroscopy
Quantum yield
Lifetime
……

## Slide 13
Excitation and Emission Spectra
Turk. J. Chem. 38(6):1083-1093 (2014).

## Slide 14
Luminescence Quantum Yield
Review of Scientific Instruments 85, 123115 (2014)
La: total # of incident photons
Lb: total # of photons not absorbed by the phosphor
Pa: dark signal in the emission wavelength area
Pb: total # of photons emitted in emission wavelength area

## Slide 15
Luminescence Lifetime
https://www.kineticriver.com/danube/
Proceedings of SPIE, 4648, April 2002. DOI: 10.1117/12.462651
https://sites.google.com/site/yichunchen52/research
https://www.lambertinstruments.com/technologies-1/2014/12/4/fluorescence-lifetime-imaging-microscopy

## Slide 16
Luminescing Materials
Tian, J Solid State Lighting, 2014, 1, 11
Optik, 2018, 153, 31-42
Objectives:
To search new host materials
To develop nanoscopic light emitters
To explore strategies to enhance luminescence
To understand structured-related mechanisms

## Slide 17
Luminescing Nanoparticles
In general and potentially:
High quantum efficiencies, sharp emission peaks, high photostability, emission wavelength tunability, and may emit light when irradiated by ionizing radiation
Bioimaging:
Organic dyes: suffer from photobleaching and broad emission
Quantum dots: exhibit toxicity
Lanthanide-doped NPs:
(1) wide excitation range: UV to NIR
(2) broad emission wavelengths
(3) enhanced photostability
(4) large Stoke’s shift
(5) increased lifetimes (milliseconds)
(6) upconversion emission, and
(7) high water dispersibility, biocompatibility, stealthy nature and preferably targeting ability
minimizes the autofluorescence and scattering of light
due to parity forbidden transitions occurring within 4f shell shielded by 5s and 5p orbitals,

## Slide 18
Outline
Intro
PL and RL
PerL
UC
Summary

## Slide 19
AIII2MIV2O7 Compounds
La2Zr2O7: ~1000ºC
Dis/ordering of cations and oxygen vacancies
fluorite < rA/rM = 1.46 < pyrochlore
Refractory with m.p. > 2500ºC
Challenge to synthesize, especially @ nanodomain
To make metastable phase if synthesis temp. is lower than phase transition temp.
One Raman peak
Six Raman peaks

## Slide 20
Benefits of the MSS Process
Lower temp. + evener distribution: Solid-state synthesis vs. MSS
Soft aggregates: sol-gel method vs. MSS
Particle size reduction: flux method vs. MSS
No milling or surface dead layer
Molten Salt Synthesis of A2M2O7 NPs
Yuanbing Mao, Xia Guo, Jian Y. Huang, Kang L. Wang, and Jane P. Chang, Luminescent nanocrystals with A2B2O7 composition synthesized by kinetically modified molten salt synthesis, Journal of Physical Chemistry C, 2009, 113(4), 1204-1208.

## Slide 21
Cationic Variation: La2Zr2O7 vs La2Hf2O7 NPs
λex = 306 nm

## Slide 22
Cationic Variation: Eu3+:La2Zr2O7 vs Eu3+:La2Hf2O7
CN | 6
40Zr: [Kr]4d25s2 | 0.72
72Hf: [Xe]4f145d26s2 | 0.71
PL: peak at ~5% Eu3+.
QY: La2Hf2O7 > La2Zr2O7.
Change of M4+ cations in ionic A2M2O7 compounds:
 Affects crystal field splitting (CFS) of Eu3+ ions
 Changes the charge cloud of Eu3+ ions
 Varies QY
Kareen Wahid, Madhab Pokhrel, and Yuanbing Mao, Structural, Photoluminescence and Radioluminescence Properties of Eu3+ Doped La2Hf2O7 Nanoparticles, Journal of Solid State Chemistry, 2017, 245, 89-97.

## Slide 23
http://research.kyoto-u.ac.jp/service/topic/spirits/lists/h25list_e/sprits_h25en_68_masai/
Medicine
Security
Expanding applications of ionizing radiation scintillation detectors
The progress on new scintillators is slow
The use of high quality single crystals is not the only way to achieve better scintillation properties
Photoluminescence vs. Radioluminescence

## Slide 24
Particle Size & Crystal Structure Engineering
Santosh K. Gupta, Maya Abdou, Partha Sarathi Ghosh, Jose P. Zuniga, and Yuanbing Mao, Thermally Induced Disorder-Order Phase Transition of Gd2Hf2O7:Eu3+ Nanoparticles and its Implication on Photo- and Radio-Luminescence, ACS Omega, 2019, 4, 2779-2791.
Tunability of RL color: red  orange
Strategy for designing advanced optoelectronic materials

## Slide 25
Core@Shell Strategy
Shell: eliminates surface defects
Charge carriers: transfer from shell to core
PL & RL: increased ~2 times
Eu:La2Zr2O7@YBO3 NPs

## Slide 26
Warm White Lighting
DOE: WLEDs will save >20% electricity (2010-30)
Deficiency of the red light component in commercial phosphors
Dy,Tb,Eu:La2Hf2O7 NPs

## Slide 27
Luminescence Thermometry
For harsh environments
High spatial resolution
Rapid response
Non-invasive operation
To reduced areas
Offering sub-​micrometric resolution
High accuracy
Current thermographic phosphors are restricted to bulk samples with moderate sensitivity and intermediate temperature range

## Slide 28
Luminescence Thermometer
Santosh K. Gupta, Jose Zuniga, P.S. Ghosh, Maya Abdou, and Yuanbing Mao, Correlating Structure and Luminescence Properties of Undoped and Eu3+ doped La2Hf2O7 Nanoparticles Prepared with Different Co-Precipitating pH Values through Experimental and Theoretical Studies, Inorganic Chemistry, 2018, 57(18), 11815-11830.
Materials | Maximum Sr (%K-1) | Temp. range (K)
Gd2O3:Er3+ /Yb3+ | 0.39 | 300-900
NaLuF4:Ho3+/Yb3+ | 0.12 | 350-750
Yb3Al5O12:Er3+ | 0.48 | 295-973
NaLuF4:Gd3+ | 0.29 | 298-523
Y2MgTiO6:Mn4+ | 0.14 | 10-513
GdVO4:Sm3+ | 1.41 | 393-603
La2Hf2O7:Eu3+ | 3.53 | 298-973
High activation energy: 0.425 eV
Highest relative temperature sensitivity (Sr)
Contributions: high QY, good PL and RL properties, high lifetime, and excellent thermal stability.
Collaborative work with Dr. Alex Puretzky at ORNL
La2Hf2O7:5%Eu NPs

## Slide 29
Nuclear Waste Immobilization
Maya Abdou, Santosh K. Gupta, Jose Zuniga, and Yuanbing Mao, On Structure and Phase Transformation of Uranium Doped La2Hf2O7 Nanoparticles as an Efficient Nuclear Waste Host, Materials Chemistry Frontiers, 2018, 2, 2201 - 2211 (cover).
Uranium and its radioactive isotopes: a high-level of nuclear waste
La2Hf2O7 NPs: U-doping induced phase transformation
Speciation studies of uranium ion in A2M2O7 compounds: uncharted and vague
Suitable properties of nuclear waste hosts:
large containing capability
high thermal stability
good radiation stability
high chemical stability
resistance to radiation-induced amorphization
negligible leaching
etc.

## Slide 30
Structural Evolution of La2Hf2O7:10%U NPs
Collaborative work with Dr. Alex Puretzky at ORNL
Cotunnite
Pyrochlore
La2Hf2O7 NPs as nuclear waste host: reversible phase transition – observed for the 1st time
Nuclear Waste Immobilization

## Slide 31
γ-ray irradiation impact on A2Hf2O7:5%Eu NPs
Collaborative work with Dr. Don Wall group at WSU
Victoria Trummel, Santosh K. Gupta, Madhab Pokhrel, Donald Wall, and Yuanbing Mao, Investigating the impact of gamma radiation on structural and optical properties of Eu3+ doped rare-earth hafnate pyrochlore nanocrystals, Journal of Luminescence, 2019, 207, 1-13.
Fascinating behavior from lanthanum (f0) hafnate and lutetium (f14) hafnate
Two extreme compositions with the maximum and minimum ionic radius ratio rRE/rHf of the studied RE2Hf2O7:5%Eu NPs
Beneficial for fundamental U chemistry and nuclear industry
Nuclear Waste Immobilization

## Slide 32
Summary on Luminescence Studies of A2M2O7 NPs
Molten-salt synthesis method for A2M2O7 NPs with different doping levels, compositions and crystal structures
Several strategies to tune the spectral features of these NPs
Explored both PL and RL of these phosphors and scintillators
Have great potentials for broad optical applications

## Slide 33
Outline
Intro
PL and RL
PerL
UC
Summary

## Slide 34
Persistent Luminescent Materials
Materials which emit in the UV, VIS and/or NIR spectral regions for minutes, hours or even days after ceasing the excitation irradiation
Bioimaging/Diagnostics
Need to avoid tissue autofluorescence and weak tissue penetration
Urgent need for PLM NPs with bright luminescence and long afterglow
To understand their biodistribution in vivo
New applications spontaneously set more requirements on design methodology, morphology, and functionalization of PLMs
New applications also promote the development of new PLMs

## Slide 35
Red Long-Lasting Phosphor Cr:ZnGa2O4
T. Maldiney, et al., Nat. Mater., 2014, 13, 418. A. Abdukayum, et al. JACS, 2013, 135, 14125.
Conveniently excited through its bandgap by UV light
Emit s around 695 nm via the 2E  4A2 transition of Cr3+
Matches the optical window of biological tissues
Use of a small dopant concentration (0.5%) and similar dopant size (Cr3+ vs Ga3+)  reduce the occurrence of defects and avoid potential loss centers
AB2O4 compound, spinel structure
Zn2+ and Ga3+ ions occupy tetrahedral A and octahedral B sites, respectively
The currently synthesized Cr:ZnGa2O4 NPs: 40–150 nm, polydisperse
No sub-10-nm persistent nanophosphors synthesized yet

## Slide 36
PerL Cr:ZnGa2O4 NPs by Bi-Phasic Synthesis

## Slide 37
Enhancing PerL of Cr3+:ZnGa2O4 NPs
Hydrothermal Synthesis
Urea + NH4NO3
Urea

## Slide 38
Outline
Intro
PL and RL
PerL
UC
Summary

## Slide 39
Upconversion Luminescence
An optical process that emits high-energy photons by absorbing two or more low-energy photons, which is caused by anti-Stokes luminescence
http://dcbwww.unibe.ch/groups/guedel/images/res/upc.GIF
Energy level
diagram
Analogy from
everyday life

## Slide 40
Enhanced Upconversion
Li+ co-doping induced phase transition
18-fold
14-fold
4S3/2→4I15/2
2H11/2→4I15/2
4F9/2→4I15/2
Er3+ ions
λex = 980 nm
Er,Yb:La2Zr2O7 NPs

## Slide 41
Upconverting Singular Red Emission

## Slide 42
Summary
Luminescent NPs of Metal Oxides
Upconversion
Persistent Luminescence
A2M2O7 NPs:
Molten-salt synthesis
6 Spectral tuning strategies
Warm white light
Luminescence thermometry
Actinide Immobilization
Er,Yb:La2Zr2O7 NPs:
Li+-co-doping
Phase-transition induced UC enhancement
Cr,Er,Yb:ZnGa2O4 NPs:
Thermal-treatment induced even distribution
Singular red emission
Cr:ZnGa2O4 NPs:
Bi-phasic synthesis
Hydrothermal synthesis
Smallest particles
Red persistent PL
Bioimaging
Photo- & Radio-Luminescence

## Slide 43: Thank you for your attention! Any questions/comments?