## Slide 1: Nanotechnology Applications E SC 215
Notes: <number>

## Slide 2
Unit 1 Material Fabrication Utilizing Plasma Enhanced Chemical Vapor Deposition (PECVD)
Lecture 1
Physical and Chemical Vapor Deposition

## Slide 3: Outline
Plasma Deposition Introduction
Deposition Coverage
The Six Basic Steps of Chemical Vapor Deposition
Film Growth
Issues Concerning PECVD Deposition
Types of PECVD Deposition

## Slide 4: Plasma Deposition Introduction
Plasma processing can be used to:
  Deposit material (PECVD)
  Remove material (etching, ashing, etc.)
  Modify the surface through bombardment
  Chemically modify the surface
These scenarios are complex chemical processes
Generally these consequences occur during any planned process, but the recipes are designed to have one result dominate

## Slide 5: Plasma Enhanced Chemical Vapor Deposition
The deposition of films using plasma offers the unique combination of low temperature and good film composition and coverage
Some PECVD systems have the ability to etch and clean the substrate prior to deposition, reducing contamination

## Slide 6
Plasma Deposition Introduction
RF power is used to break up gas molecules in a vacuum
Molecular fragments (radicals) readily bond to other atoms to form a film at the substrate’s surface
Gaseous by-products are removed by the vacuum pumping system
The substrate may be heated to increase surface reactions and drive out contaminants

## Slide 7: Outline
Plasma Deposition Introduction
Deposition Coverage
The Six Basic Steps of Chemical Vapor Deposition
Film Growth
Issues Concerning PECVD Deposition
Types of PECVD Deposition

## Slide 8: Deposition Step Coverage
A key quality issue in deposition is step coverage
  The thickness of a deposited material over features relative to the thickness on the top surface

## Slide 9: Step Coverage
Sidewall Step Coverage = 100 x a/b (%)
Bottom Step Coverage = 100 x d/b (%)
Conformality = 100 x a/c (%)
a
b
c
d
Public Domain: Image Generated by CNEU Staff for free use

## Slide 10: Deposition Uniformity
Insuring uniform coverage
  The substrate chuck is heated to control the morphology of the deposition
  Plasma ion bombardment is also used to increase the mobility of adatoms

## Slide 11: Outline
Plasma Deposition Introduction
Deposition Coverage
The Six Basic Steps of Chemical Vapor Deposition
Film Growth
Issues Concerning PECVD Deposition
Types of PECVD Deposition

## Slide 12: Chemical Vapor Deposition Model
Vapor (bulk gas) diffusion
Adsorption of film precursor
Surface diffusion
Nucleation and island growth
Desorption of reaction products
Diffusion of reaction products into the bulk gas

## Slide 13
“Gas phase nucleation”
Stagnant layer
1. Precursor
diffusion
2. Adsorption of film precursor
3. Surface
diffusion
4. Nucleation
and island growth
5.Desorption of
reaction products
Precursor
desorption
Film growth
Reactant 1
Reactant 2
Byproduct of Reaction
Public Domain: Image Generated by CNEU Staff for free use
6. Diffusion of reaction products into the bulk for pump out

## Slide 14: Outline
Plasma Deposition Introduction
Deposition Coverage
The Six Basic Steps of Chemical Vapor Deposition
Film Growth
Issues Concerning PECVD Deposition
Types of PECVD Deposition

## Slide 15: Forming a Film
Given enough time and surface mobility, a deposited film grows in three stages
  Nucleation
  Island growth
  Coalescence

## Slide 16: Nucleation
The first stage of thin film growth where clusters of stable nuclei are formed on the substrate’s surface
Public Domain: Image Generated by CNEU Staff for free use

## Slide 17: Island Growth
The second stage of thin film growth where stable nuclei grow into larger island clusters based on surface mobility and density
Public Domain: Image Generated by CNEU Staff for free use

## Slide 18: Coalescence
The final stage of thin film growth where island clusters coalesce, or combine, eventually forming a continuous film
Public Domain: Image Generated by CNEU Staff for free use

## Slide 19: Outline
Plasma Deposition Introduction
Deposition Coverage
The Six Basic Steps of Chemical Vapor Deposition
Film Growth
Issues Concerning PECVD Deposition
Types of PECVD Deposition

## Slide 20: Quality Issues in CVD
Film Density
Film Stress
Included Contaminants
Surface Damage

## Slide 21: Advantages of PECVD
Lower processing temperature (~150 to 450oC), gives a wide range of applications
Excellent gap-fill for high aspect ratio gaps (low density plasma)
Good film adhesion to the substrate
High deposition rates
Can have high film density due to few pinholes and voids

## Slide 22: PECVD Limitations
Besides the expected substrate damage due to ion bombardment, PECVD has a tendency to create voids in trenches
Void creation is a function of Mean Free Path
Key-hole defect
Public Domain: Image Generated by CNEU Staff for free use

## Slide 23: Voids and MFP
D
W
Balanced mean free
path, rapid surface
migration
Long mean free path, no surface migration
Short mean free path, no surface migration
Public Domain: Image Generated by CNEU Staff for free use

## Slide 24: Plasma Deposition and Photoresist
Unlike etching, photoresist is undesirable for plasma depositions
  Besides thermal flow due to a heated substrate chuck, plasma will react with the photoresist resulting in a volatile product that contaminates the film

## Slide 25: Plasma Deposition and Photoresist
Plasma
Substrate
Film
PR
PR
Deposited Film
Photoresist reacting
with plasma
Contaminated film
Public Domain: Image Generated by CNEU Staff for free use

## Slide 26: Outline
Plasma Deposition Introduction
Deposition Coverage
The Six Basic Steps of Chemical Vapor Deposition
Film Growth
Issues Concerning PECVD Deposition
Types of PECVD Deposition

## Slide 27: PECVD Films
Polysilicon | Used as a gate material in semiconductor devices, and as a flexible material for MEMS
Silicon Nitride | Diffusion barrier
Silicon Dioxide | Dielectric layer
Borosilicate glass | BSG
Phosphosilicate glass | PSG
Boro-phospho-silicate glass | BPSG
Tungsten(W) | Used for via fill or barrier metal
Copper(Cu) | Replacing aluminum as metal conductor in devices
Public Domain: Image Generated by CNEU Staff for free use

## Slide 28: Polysilicon PECVD
Polysilicon contains many small single-crystal regions separated by grain boundaries
Doped polysilicon serves as a gate electrode in MOS devices
Polysilicon is also popular as a flexible material for MEMS applications

## Slide 29: Polysilicon PECVD
Polysilicon is deposited in PECVD by a decomposition reaction
Silane (SiH4), upon exposure to RF, decomposes into solid silicon and hydrogen gas
The substrate chuck is heated to above 580oc to insure the proper polycrystalline structure is realized
SiH4 (gas)  Si (solid) + 2H2 (gas)

## Slide 30: Nanocrystalline Silicon (nc-Si)
nc-Si has small grains of crystalline silicon within the amorphous phase
The grains are less than 100nm
Behaves like a discrete gap semiconductor
nc-Si has electron mobility much greater than that of amorphous silicon (a-Si)
Has found use in solar cells due to its strong light absorption properties

## Slide 31: Silicon Nitride PECVD
Nitride is used as:
  A final passivation layer on chips for scratch protection
  A moisture barrier
  Radiation shielding
  A barrier against Na diffusion
PECVD nitride contains hydrogen (9-30%), this can degrade the film
PECVD nitride is also exposed to greater compressive stress due to ion bombardment, causing voids and cracks in underlying layers

## Slide 32: Silicon Nitride: PECVD VS LPCVD
Property | LPCVD | PECVD
Deposition Temperature(oC) | 700 to 800 | 300 to 400
Composition | Si3N4 | SixHyNz
Step Coverage | Fair | Conformal
Stress at 23oC on silicon (dynes/cm2) | 1.2-1.8 x 1010 (Tensile) | 1-8 x 109 (compressive and tensile)
Andrzej Mieckowski Penn State Nanofabrication Facility

## Slide 33: Silicon Nitride PECVD
PECVD nitride is formed by reacting silane with either ammonia (NH3) or nitrogen(N2)
  Using N2 reduces the amount of hydrogen in the film, but is difficult to dissociate.
SiH4(gas)+NH3(gas)SixHyNz(solid)+H2(gas)
SiH4(gas)+N2(gas)SixHyNz(solid)+H2(gas)

## Slide 34: Example Nitride PECVD Recipe
Step | Time (Sec) | Pres (Torr) | Cham Temp (oC) | Subs Temp (oC) |  | Power (W) | N2 (SCCM) | NH3 (SCCM) | SiH4 (SCCM)
1 | 10 | 4.0 | 410 | 325 |  | 0 | 4000 | 275 | 60
2 | 2 | 4.0 | 410 | 372 |  | 500 | 4000 | 275 | 60
3 | 25 | 4.25 | 410 | 353 |  | 640 | 4000 | 100 | 285
4 | 44 | 4.25 | 410 | 379 |  | 640 | 4000 | 100 | 285
5 | 10 | 0.3 | 410 | 377 |  | 50 | 2500 | 0 | 0
6 | 10 | 0.3 | 410 | 375 |  | 0 | 0 | 0 | 0
Andrzej Mieckowski Penn State Nanofabrication Facility

## Slide 35: Silicon Dioxide PECVD
Oxide is formed by reacting silane (SiH4) with either oxygen(O2), nitrous oxide(N2O), or carbon dioxide(CO2) in a plasma
Oxide can also be doped with boron(B2H6) or phosphorous(PH3) to form BSG or PSG respectively

## Slide 36: Silicon Dioxide PECVD
O2 is generally not used due to its ability to readily react in the gas phase, generating particles that promote poor film quality
N2O is the preferred reactant due to its ability to produce a higher quality film
SiH4(gas)+2N2O(gas)SiO2(solid)+2N2(gas)+2H2(gas)

## Slide 37: Tungsten PECVD
Tungsten is a refractory metal (mp = 3410 °C) widely used in multilevel metal structures as an interconnect and a barrier metal
Tungsten qualities
  High conductivity
  Excellent thermal capabilities
  Good CVD step coverage

## Slide 38: Tungsten PECVD
Tungsten deposition via PECVD is a fairly simple process
Tungsten hexafluoride (WF6) reacts with hydrogen to form solid tungsten and hydrofluoric acid vapor
WF6(gas) + 3H2(gas)  W(solid) + 6HF(gas)

## Slide 39: Copper PECVD
Copper is replacing aluminum as the metal conductor of choice in high speed devices
Copper qualities
  Excellent conductivity
  Low production cost
  Good step coverage

## Slide 40: Copper PECVD
Copper PECVD is the most common method of deposition
The metal organic bis-hexafluoroacetyl-acetonate-CuII, written as Cu(hfac)2 is placed into the system in powder form and is mixed with hydrogen gas and then vaporized and carried into the reaction chamber
Cu(hfac)2 + H2  Cu + 2H(hfac)