## Slide 1: Nanotechnology Applications E SC 215
Notes: <number>

## Slide 2
Unit 2 Material Fabrication Utilizing Dry Etch Chemistry
Lecture 2
Plasma Removal Process

## Slide 3: Outline
Introduction
Models to understand the plasma process
Chemistry
Analyzing recipe parameters, and the resultant etch profiles
Endpoint

## Slide 4: Introduction
Reactive Ion Etching (RIE): An etch process where a substrate is placed on an RF-powered electrode to achieve a chemical and physical etch
Aspect Ratio: The ratio of the depth to width for a small gap, tech, or hole.
DC Bias: A DC volt that develops across a plasma process chamber when an RF voltage is applied to the chamber's electrodes.
Mean Free Path: The average distance an atom or molecule travels before striking another atom or molecule.
Radicals: Molecules or fragments that contain unsatisfied bonds (unpaired electrons). They are extremely reactive.

## Slide 5: Introduction
Ions: Are atoms, molecules or pieces of molecules that have gained or lost electrons. They can be negatively (anions) or positively charged (cations).
Etch Rate: The speed at which a material is removed from a substrate during etching
Residence Time: The average time gas (etch chemistry, byproducts) is present in a vacuum chamber
Dark Sheath: Area adjacent to plasma generating electrodes that appears darker than the rest of the plasma (glow region). The dark sheath (or ion sheath) is a result of a lack of electrons and has a stronger electric field as well as less resistance compared to the glow region
Sheath Potential: The potential difference between the glow region of the plasma and the cathode in a dry etch system

## Slide 6
Limits of Wet Etch Illustrates the Need for Plasma Processing
Wet etching is limited to ~ 2-3 µm pattern features due to liquid trapping / surface tension (dependent upon materials)
Wet etching tends to undercut and produce sloped sidewalls
Wet etching needs rinse and dry steps
Wet chemicals can be hazardous, toxic and expensive (environmental concerns)
Wet processes present material contamination issues

## Slide 7: Plasma Etching
Plasma etching is a balance between:
  Selective removal (what is intended vs. what is protected) of material through chemical reactions
  Nonselective removal of material through ion bombardment (pressure and power related)
  Deposition of sidewall polymers for passivation
  Varying these parameters determines the etch profile

## Slide 8
Plasma
Within a plasma, there are a number of species
  Radicals
  Ions
  Neutrals
  Electrons
  Film formers
    if desired, for sidewall passivation in etch processes
  Diluents

## Slide 9
Contents of a Plasma
A dry plasma etch may contain:
  Radicals that chemically react with the substrate and selectively remove material
  Ions that remove material through physical bombardment (no selectivity) and provide uniformity
  Neutrals
  Electrons aid in sustaining the plasma
  Film formers that provide sidewall passivation (optional)
  Diluents- an inert gas introduced into the reaction chamber along with the process gasses to maintain the desired reaction rate (optional)

## Slide 10: Selective Etching
Etching that is done so that certain material is removed, but other materials or areas of the materials are ideally not affected
Selective etching is difficult to achieve when chemically different layers form similar etch products
  Example: SiO2, Si, and Si3N4 each form SiF4 during the etching process ( selectivity)

## Slide 11
Outline
Introduction
Models to understand the plasma process
Chemistry
Analyzing recipe parameters, and the resultant etch profiles
Endpoint

## Slide 12
Plasma Glow Region
Electrons
Radicals
Ions
Film Formers
Neutrals
Sheath Dark Space
Neutral Transport-Diffusion
Ion Acceleration
Surface Interactions
Substrate
Simplified
Plasma Model
Public Domain: Image Generated by CNEU Staff for free use

## Slide 13
Ions vs. Radicals in a Plasma
Radicals are molecules or pieces of molecules that contain unsatisfied bonds (unpaired electrons)
Ions are molecules or pieces of molecules that are negatively or positively charged. We generally are concerned with the positive ions for focused bombardment, because they can be easily drawn to the cathode which holds the sample

## Slide 14
Plasma in Terms of Temperature, Chemistry, and Bombardment
Chemistry = Selectivity
  Radicals react with surface to form volatile etch products that are pumped away
  Selectivity, properly tuned chemistry can result in some materials being etched more than others
Bombardment = Uniformity
  Ions accelerated by the voltage difference between the plasma and the surface being etched strike the substrate and remove material by kinetic energy. Bombardment energy also aids surface chemical reactions. Bombardment is a power and pressure regulated process
Temperature = Rate
  Average plasma temperature (for a low density plasma) is about 100oC plus room temperature, low enough for virtually any process, including photoresist
Etch profile is a result of the energies at the substrate. C*B+T

## Slide 15
Pressure
Pressure has the largest impact on plasma etching. It is the “big control knob”
Pressure affects:
  Mean free path (MFP)
  Collisions at the material interface (substrate)
  Etch profile: isotropic or anisotropic
  Residence time
  Microloading

## Slide 16: Pressure
Pressure affects the MFP, which controls, among other things, the degree of ionization and thus the number of ions available for physical bombardment
MFP (bombardment) gets larger as pressure is reduced, naturally the amount of chemistry (etching gas, etch byproducts) is reduced when the pressure is decreased
A low pressure will increase bombardment, and uniformity, but decrease selectivity
A high pressure will decrease bombardment, and decrease uniformity, but will generally increase selectivity

## Slide 17: The “Wine Glass” Etch Profile (RIE)
PR
Substrate
Isotropic Etch Profile —Generally 100’s mT
Anisotropic Etch Profile —Generally 10’s mT
Public Domain: Image Generated by CNEU Staff for free use

## Slide 18: Power
Power also affects ionization
As power increases, ionization increases
Power and pressure are inter-related: the effect of power depends on the operating pressure.

## Slide 19: Minimum Energy Required to Ionize a Particle
Particle | Energy(eV) | Particle | Energy(eV)
H | 13.5 | H2 | 15.4
He | 24.5 | N2 | 15.5
N | 14.5 | O2 | 12.2
O | 13.5 | Cl2 | 12
F | 17.4 | Br2 | 11
Cl | 13 | BCl3 | 11
Ar | 15.7 |  | 

## Slide 20: Process Variation Affects
Power = Sheath potential e- velocity Ions and radicals Etch rate Selectivity
Pressure = Etch rate
Area exposed to etching = Etch rate
Electrode spacing = Ion energy Ion density

## Slide 21
The Six Steps of Plasma Etching
Reactive etching species are generated by electron/molecule collisions
Etchant species diffuse through stagnant region to the surface of the film to be etched
Etchant species adsorb onto surface (ion bombardment can help provide energy to drive chemical reactions)
Reaction takes place at the surface
Etched product desorbs from the surface (ion bombardment can help provide energy for desorption)
Etch products diffuse back into bulk gas and are removed by vacuum

## Slide 22
Gas Flow
1. Generation of plasma species
2. Etchant species
diffusion
3. Adsorption
4. Reaction
Substrate
Volatile
product
5. Desorption
6. Diffusion into
bulk gas
Public Domain: Image Generated by CNEU Staff for free use

## Slide 23: Sidewall Passivation
Sidewall passivation can be used in an etch process to control sidewall profile
A film forms on the sidewalls, preventing the material from being etched isotropically
The film is actually a polymer formed from the process gases and the photoresist layer on the substrate
The polymers are basically combinations of carbon and hydrogen. May contain oxygen and nitrogen and other etch byproducts. Polymer chemistry depends on process conditions.
Specific gases can be added to the recipe to insure passivation film formation

## Slide 24: Etch Profile with Sidewall Passivation
Radicals: reactive etching species
Reaction Products: volatile etch products
Film formers: provide sidewall passivation, photoresist can be a large contributor
Positive ions: provide physical bombardment on surface, breaking surface film formers at bottom, physically etching and providing energy to help drive chemical reactions
Public Domain: Image Generated by CNEU Staff for free use

## Slide 25: Sidewall Passivation
Polymers coat the sidewalls and act as a “pseudo-mask” for protection from chemical attack
Ions, for the most part, strike vertically and remove polymer buildup at the bottom of the etch
The sidewall polymers are removed by using O2 plasma at 500-750mT
  This exposure uses a lot of chemistry and little bombardment

## Slide 26
Outline
Introduction
Models to understand the plasma process
Chemistry
Analyzing recipe parameters, and the resultant etch profiles
Endpoint

## Slide 27
Controlling the Etch Process by Balancing Chemistry and Bombardment
In dry etch processes choosing the correct chemistries can greatly increase the etch rate
Increasing MFP of the plasma (decreasing the pressure) also increases the etch rate, this will aid uniformity
Combining chemistry and bombardment will produce an etch rate that is greater than either contributor alone
Combining chemistry and bombardment allows the profile to be “tuned” between isotropic and anisotropic
The etch profile can also be enhanced with side wall passivation

## Slide 28: Example Sidewall Chemistries
Material | Chemistry | Volatile Etch Product | Sidewall Material
Oxide Etch | SiO2 + CF4 + CHF3 + Ar  | SiF, SiOF, SiF4, SiH4 | Si, C, CHx, F 
Poly Si Etch | Si + HBr + Cl2  | SiBrx  SiClx | Si,Br,C,Cl 
Al Etch | Al + BCl3 + Cl2 + N2  | AlCl3  | Al,B,C,N,Cl 

## Slide 29: Variations in Oxide Etch
Increase In: | Etch Rate of SiO2 | Selectivity to Silicon | Uniformity
Ion Energy |  |  | 
O2 Level in Process |  |  | 
H2 Level in Process |  |  | 
SiO2 Dopant Level |  |  | 
Silicon Dopant Level |  |  | 

## Slide 30
Formula | Common Name | Chemical Name | Formula | Chemical Name
CF4 | Freon 14 | Tetrafluoro-methane | SiCl4 | Silicon Tetrachloride
C2F6 | Freon 116 | Perfluoro-ethane | BCl3 | Boron-trichloride
C3F8 | Freon 218 | Perfluoro-propane | Cl2 | Chlorine
CHF3 | Freon 23 | Trifluoro-methane | HCl | Hydrogen Chloride
CF3Br | Freon 13B1 | Bromo- trifluoro-methane | HBr | Hydrogen Bromide
SF6 |  | Sulfur Hexafluoride | He | Helium
NF3 |  | Nitrogen Trifluoride | N2 | Nitrogen
SiF4 |  | Silicon Tetrafluoride | O2 | Oxygen
Some etching Gases

## Slide 31
PolySilicon | Cl2 or BCl3/CCl4 HBr /CF4 /CHCl3 /CHF3 | WSi2,TiSi2,CoSi2 | CCl2F3
Aluminum | Cl2 BCl3 + passivating gases SiCl4 | Single crystal Si | Cl2 or BCl3 + passivating gases
AlSi(1%)-Cu(0.5%) | same as Al | SiO2 (BPSG) | CCl2F2,CF4,C2F6, C3F8
Al-Cu(2%) | BCl3/Cl2/CHF3 | Si3N4 | CCl2F2 CHF3
Tungsten | SF6/Cl2/CCl4 | GaAs | CCl2F2
TiW | SF6/Cl2/O2 |  | 
Material
Chemistry
Chemistry
Material
Some Materials and Selected Etchants

## Slide 32
Outline
Introduction
Models to understand the plasma process
Chemistry
Analyzing recipe parameters and the resultant etch profiles
Endpoint

## Slide 33: The “Egg” Chart
This analytical model is a graphical representation of various process parameters. The Y axis represents bombardment energy, the X axis represents chemical energy, and the “dog leg” boundary represents polymer formation.
For an ideal anisotropic etch, the required parameter zone resembles an “egg” in the middle of the chart
This chart shows the combined effects of chemistry, bombardment, and polymerization (C*B+P) to predict sidewall profiles
There are also other factors that determine the etch profile that are not included in this exercise. These parameters will be discussed after this first iteration analysis.

## Slide 34: The “Egg” Chart
A chart like this can be found and/or generated for any dry etchable material
Due to its wide use in micro and nanofabrication, we will analyze the egg chart for SiO2
Naturally this chart is not “exact”, but can be used as a starting point for building a etch recipe.

## Slide 35: Oxide Egg Chart Considerations
F/C Ratio- the ratio of fluorine to carbon etching species
Increasing DC bias, increases bombardment
The addition of H2 to the chamber increases polymerization
The addition of O2 to the chamber increases free fluorine
Aspect Ratio- the ratio of depth to width for a small gap, trench, or hole

## Slide 36
0
1
2
3
4
Fluorine to Carbon Ratio (F/C) of Gas Phase Etching Species vs DC Bias Level
Bias Applied to Surface (Volts)
DC Bias
Low
High
Polymerization
Etching
O2 Addition
Loading
H2 Addition
C2F4
C4F10
C2F6
CF4
F/C Ratio
Public Domain: Image Generated by CNEU Staff for free use

## Slide 37
0
1
2
3
4
Fluorine to Carbon Ratio (F/C) of Gas Phase Etching Species vs DC Bias Level
Bias Applied to Surface (Volts)
DC Bias
Low
High
Polymerization
Etching
O2 Addition
Loading
H2 Addition
C2F4
C4F10
C2F6
CF4
F/C Ratio
Public Domain: Image Generated by CNEU Staff for free use
1

## Slide 38: The Ideal Profile
To be “in the egg” is to achieve the ideal anisotropic etch
  The ideal F/C ratio is approximately 2
  An equal mix of hydrogen and oxygen to balance polymerization and etch
  DC bias level that provides just enough bombardment

## Slide 39: The Ideal Profile
D
W
Public Domain: Image Generated by CNEU Staff for free use

## Slide 40: Sidewall Profile Two
Low DC bias – little/no bombardment
No H2 - no polymerization
A lot of O2 – can increase etching
F/C ratio = 4, SiF4 is formed
Aspect ratio < 1, an isotropic etch profile

## Slide 41
0
1
2
3
4
Fluorine to Carbon Ratio (F/C) of Gas Phase Etching Species vs DC Bias Level
Bias Applied to Surface (Volts)
DC Bias
Low
High
Polymerization
Etching
O2 Addition
Loading
H2 Addition
C2F4
C4F10
C2F6
CF4
F/C Ratio
Public Domain: Image Generated by CNEU Staff for free use
2

## Slide 42: Sidewall Profile Two
Public Domain: Image Generated by CNEU Staff for free use

## Slide 43: Sidewall Profile Three
Low DC bias – no bombardment
A lot of H2 - a lot of polymerization
No O2 – no etch
F/C = 1/3, SiF4 is not formed

## Slide 44
0
1
2
3
4
Fluorine to Carbon Ratio (F/C) of Gas Phase Etching Species vs DC Bias Level
Bias Applied to Surface (Volts)
DC Bias
Low
High
Polymerization
Etching
O2 Addition
Loading
H2 Addition
C2F4
C4F10
C2F6
CF4
F/C Ratio
Public Domain: Image Generated by CNEU Staff for free use
3

## Slide 45: Sidewall Profile Three
Polymer buildup
Public Domain: Image Generated by CNEU Staff for free use

## Slide 46: Sidewall Profile Four
High DC bias – high bombardment
No H2 – no polymerization
A lot of O2 – high etch
F/C ratio = 4, SiF4 is formed
Aspect ratio >1, a dry etch profile

## Slide 47
0
1
2
3
4
Fluorine to Carbon Ratio (F/C) of Gas Phase Etching Species vs DC Bias Level
Bias Applied to Surface (Volts)
DC Bias
Low
High
Polymerization
Etching
O2 Addition
Loading
H2 Addition
C2F4
C4F10
C2F6
CF4
F/C Ratio
Public Domain: Image Generated by CNEU Staff for free use
4

## Slide 48: Sidewall Profile Four
6
3
Sharp angles due
to high bombardment
with no polymerization
Public Domain: Image Generated by CNEU Staff for free use

## Slide 49: Sidewall Profile Five
High DC bias – high bombardment
A lot of H2 – a lot of polymerization
No O2 – no etch
F/C ratio =1/5, SiF4 is not formed
Aspect ratio > 1, Dry etch profile with undesirable features

## Slide 50
0
1
2
3
4
Fluorine to Carbon Ratio (F/C) of Gas Phase Etching Species vs DC Bias Level
Bias Applied to Surface (Volts)
DC Bias
Low
High
Polymerization
Etching
O2 Addition
Loading
H2 Addition
C2F4
C4F10
C2F6
CF4
F/C Ratio
Public Domain: Image Generated by CNEU Staff for free use
5

## Slide 51: Sidewall Profile Five
Jagged features
due to
polymer buildup
Public Domain: Image Generated by CNEU Staff for free use

## Slide 52: Sidewall Profile Six
Medium DC bias – medium bombardment
No H2 – no polymerization
A lot of O2 – high etch
F/C = 4, SiF4 is formed
Aspect ratio < 1, a wet etch profile

## Slide 53
0
1
2
3
4
Fluorine to Carbon Ratio (F/C) of Gas Phase Etching Species vs DC Bias Level
Bias Applied to Surface (Volts)
DC Bias
Low
High
Polymerization
Etching
O2 Addition
Loading
H2 Addition
C2F4
C4F10
C2F6
CF4
F/C Ratio
6
Public Domain: Image Generated by CNEU Staff for free use

## Slide 54: Sidewall Profile Six
Wider and deeper
than profile one
due to increased
bombardment
Public Domain: Image Generated by CNEU Staff for free use

## Slide 55: Sidewall Profile Seven
Medium DC bias – medium bombardment
A lot of H2 – a lot of polymerization
No O2 – no etch
F/C ratio = ¼, SiF4 is not formed
Aspect ratio > 1, Dry etch profile with undesirable features

## Slide 56
0
1
2
3
4
Fluorine to Carbon Ratio (F/C) of Gas Phase Etching Species vs DC Bias Level
Bias Applied to Surface (Volts)
DC Bias
Low
High
Polymerization
Etching
O2 Addition
Loading
H2 Addition
C2F4
C4F10
C2F6
CF4
F/C Ratio
7
Public Domain: Image Generated by CNEU Staff for free use

## Slide 57: Sidewall Profile Seven
Less bombardment than profile four
Public Domain: Image Generated by CNEU Staff for free use

## Slide 58
Considerations Beyond
the Egg Chart
The “egg chart” is a useful first approximation to define some process parameters, but it does not cover some important considerations.
We will discuss 4 additional considerations:
  Residence time
  Microloading
  Proximity effect
  Post etch evaluation

## Slide 59
Residence Time
The average time gas is present in the chamber (seconds)
The residence time is a balance of the pressure, input gas flow, and the pump efficiency
Naturally the residence time will impact the etch process, because etch chemistry and byproducts are constantly being pumped away at a certain rate

## Slide 60
Microloading
The change in local etch rate relative to the whole area of material being etched
  A large area will load the etching process with volatile etch products, slowing the etch down in that area while a smaller etch area proceeds at a faster rate
Etch rates change according to pattern and exposed area

## Slide 61
Microloading
Larger area loading
the process with removed
material- less etching gas
relative to area
More etching
gas relative to area-
etches quicker
Photoresist on top of Wafer
Patterned holes in the PR where etching of the wafer occurs
Public Domain: Image Generated by CNEU Staff for free use

## Slide 62
Proximity Effect- Etch Rate Based on Feature Size
Si
Si
F
SiF4
“Crowded”-
harder to remove byproducts,
slower etch rate
Si
Si
F
SiF4
Easier to remove byproducts,
faster etch rate
Public Domain: Image Generated by CNEU Staff for free use

## Slide 63
Etch Evaluation
Process quality parameters:
  Etch rate, selectivity, uniformity
  Sidewall Profile
  Loss or gain of critical dimensions
  Corrosion (in metal etch)
  Reproducibility

## Slide 64
Outline
Introduction
Models to understand the plasma process
Chemistry
Analyzing recipe parameters, and the resultant etch profiles
Endpoint

## Slide 65: Endpoint Detection
General term describing when an etch process has finished
Two common methods of detection
  Optical emission
  Mass spectroscopy

## Slide 66: Optical Emission
Each volatile etch product emits a specific wavelength
The wavelength intensity shows the relative amounts of products being formed
A decrease in intensity corresponds to a decrease in etch products.

## Slide 67: RIE With Optical Endpoint Detector
Endpoint Detector
Oxford Instruments Plasmalab System 100
Public Domain: Image Generated by CNEU Staff for free use

## Slide 68
Material to be etched Etchant Gases Emitting Species (nm)
Silicon CF4/O2;SF F(product) 704
CF4/O2;SF SiF(product) 440,777
Cl2 SiCl(product) 287
SiO2 CHF3 CO(product) 484
Si3N4 CF4/O2 N2(product) 337
CF4/O2 CN(product) 387
CF4/O2 N(product) 674
CF4/O2 F(etchant) 704
Al Cl2;BCl3 Al(product) 391,394,396
Cl2;BCl3 AlCl(product) 261
Resist O2 O(etchant) 777,843
O2 CO(product) 484
O2 OH(product) 309
O2 H(product) 656
Optical Emission

## Slide 69: Example Graph of Optical Endpoint Detection
Endpoint detection
Normal etch
Change in etch rate - detection occurs here.
Endpoint signal stops the etch.
Time
Etch Parameter
Public Domain: Image Generated by CNEU Staff for free use

## Slide 70: Mass Spectroscopy
This method of endpoint detection measures the mass/charge ratio of the etch products
As the mass/charge ratio peak declines, the products being generated by the etch decline due to the material being etched away
A residual gas analyzer is a mass spectrometer
Notes: <number>

## Slide 71: Mass Spectrometer Schematic
Detector
Steering magnets
Particle Accelerator
Ionizing electron stream
A
Public Domain: Image Generated by CNEU Staff for free use

## Slide 72: Example Mass Spectra: Benzyl Alcohol
Benzyl Alcohol
Public Domain: Image Generated by CNEU Staff for free use