## Slide 1: Nanotechnology Applications E SC 215
Notes: <number>

## Slide 2
Unit 4 Oxidation and Dielectric Materials
Lecture 1
Dielectrics by Growth and Deposition

## Slide 3: Outline
Introduction – Silicon Dioxide
Types of Oxide
Furnace Deposition
  Dry Oxidation
  Wet Oxidation
High Pressure Oxidation
Chemical Vapor Deposition
Modifying Dielectric Constant

## Slide 4: Oxidation
Oxidation is a chemical reaction in which silicon and oxygen form a stable material called silicon dioxide.

## Slide 5: Silicon Dioxide
A high quality, stable electrical insulator material
Grows naturally on silicon
Has many uses

## Slide 6: Silicon Dioxide
SiO2
Oxide Lattice
Tetrahedral
Structure of oxide
Si
Oxygen
Key:
Public Domain: Image generated by CNEU Staff for free use

## Slide 7: Oxide Quality
Determined by checking:
  Film thickness and uniformity (nm)
  Defects (#/volume)
  Dielectric strength (MV/cm2)
  Stress (MPa)
  Interface properties

## Slide 8: Film Thickness
Oxide film thickness can be roughly judged by the color of the oxide.
This is a general measurement, but can be useful.

## Slide 9
Thickness | Color | Thickness | Color
0.05 μm | Tan | 0.54 | Yellow-green
0.12 | Royal Blue | 0.57 | Yellow to “yellowish”
0.17 | Metallic to v. light yellow-green | 0.60 | Carnation Pink
0.22 | Gold w/ orange-yellow | 0.63 | Violet-red
0.27 | Red-violet | 0.80 | Orange
0.32 | Blue to Blue-green | 0.85 | Dull, light Red-violet
0.36 | Yellow-green | 0.87 | Blue-violet
0.39 | Yellow | 0.92 | Blue-green
0.42 | Carnation Pink | 0.97 | Yellow to “yellowish”
0.50 | Blue-green | 1.00 | Carnation Pink
Silicon Dioxide Thickness

## Slide 10: Mechanism
Oxygen moves through the oxide layer to react with the silicon below.
Oxygen diffuses from an area of high concentration (gas) to an area of low oxygen conc. (silicon).
Fick’s first law states that the particle flow per unit area, J (particle flux), is directly proportional to the concentration gradient of the particle:
  J = -D∂N(x,t)/∂x

## Slide 11: Diffusion of Oxygen
O2
SiO2
Si
Public Domain: Image generated by CNEU Staff for free use

## Slide 12: Mechanism
Silicon in the wafer is consumed as the oxide grows.
Typically, for every 1000Å of oxide grown, 400Å of silicon is consumed.
For a 1000Å layer of oxide, the wafer physically grows only 600Å.

## Slide 13: Outline
Introduction – Silicon dioxide
Types of Oxide
Furnace Deposition
  Dry Oxidation
  Wet Oxidation
High Pressure Oxidation
Chemical Vapor Deposition
Modifying Dielectric Constant

## Slide 14: Types of Oxides
Native Oxide
  Considered a contaminant. It grows naturally on silicon at room temperature due to the presence of O2 in the ambient environment.
  Can reach a maximum thickness of ~40Å.
Gate Oxide
  A highly pure, specifically grown oxide that acts as a dielectric between the gate, source, and drain on the MOS structure.
  Optimal thickness is between 20Å and several hundred Å.
  Higher purity and thinner oxides lead to the production of faster devices.

## Slide 15: Types of Oxide
Gate Oxide
p+ Si
SiO2 Native Oxide (200nm)
p+ Si
Gate
Drain
Source
Gate Oxide
Native Oxide
Public Domain: Image generated by CNEU Staff for free use

## Slide 16: Types of Oxide
Field Oxide (FOX)
  Used to isolate individual transistors from each other on a wafer
  Ideal thickness is between 2,500Å – 15,000Å.
Barrier Oxide
  Protects active devices and silicon from further processing
  Ideal thickness is usually several hundred Å

## Slide 17: Types of Oxide
Barrier Oxide
p+ Si
Gate
Drain
Source
Field Oxide
Field Oxide
p+ Si
Gate
Drain
Source
Barrier Oxide
Public Domain: Image generated by CNEU Staff for free use

## Slide 18: Types of Oxide
Barrier
  Used as a mask to prevent doping in unwanted areas
  Also used in patterning of wafers. Its chemical resistance provides a strong barrier for etching/depositing/etc. patterns in a wafer
  Optimal thickness ~400Å – 1,200Å, but it depends on the doping process.
Pad Oxide
  Reduces stress for Si3N4
  Thickness is kept very thin.

## Slide 19: Types of Oxide
Pad Oxide
p+ Si
Dopant Barrier Oxide
Pad Oxide
Dopant Barrier Oxide
p+ Si
Gate
Drain
Source
Public Domain: Image generated by CNEU Staff for free use

## Slide 20: Types of Oxide
Implant Screen Oxide
  Used to prevent/minimize implant channeling and damage.
  Thickness varies depending on implant depth.
Insulating Barrier
  Placed between metal layers to prevent electrical shorts
  Used because of its insulating properties (does not conduct electricity)
  This layer is deposited (as opposed to grown) and the required thickness varies.

## Slide 21: Types of Oxide
Insulating Barrier Oxide
Si
Implant Screen Oxide
Screen Oxide
p+ Si
Gate
Drain
Source
Metal 2
Metal 1
Insulating barrier oxide
Public Domain: Image generated by CNEU Staff for free use

## Slide 22: Outline
Introduction – Silicon dioxide
Types of Oxide
Furnace Deposition
  Dry Oxidation
  Wet Oxidation
High Pressure Oxidation
Chemical Vapor Deposition
Modifying Dielectric Constant

## Slide 23: Oxidation
Three methods for growing oxide:
  High temperature oxidation (furnace)
    w/ oxygen: dry oxidation
    w/ steam: wet oxidation
  High-pressure oxidation – HiPOx
One method of depositing oxide:
  CVD – chemical vapor deposition

## Slide 24: Furnace Oxidation
Important parameters for furnace processes:
  Time
  Temperature
  Temperature gradients
  Gas composition and purity
  Gas flow rate
  Thermal stress management

## Slide 25: Outline
Introduction – Silicon dioxide
Types of Oxide
Furnace Deposition
  Dry Oxidation
  Wet Oxidation
High Pressure Oxidation
Chemical Vapor Deposition

## Slide 26: Dry Oxidation
Oxidation that occurs as a result of oxygen reacting with silicon
  Si + O2  SiO2
Grows high quality thin layers of oxide (i.e. gate oxides)
Grows oxide at a slow rate.

## Slide 27: Dry Oxidation
The process is performed in the furnace at a high temperature (normally above 1000oC)
Uses oxygen as the process gas
May use HCl in process to reduce charges at the wafer surface.

## Slide 28: Dry Ox. Process Recipe
Step | Time (min) | Temp. (°C) | Gas Flow (SLM) |  | 
 |  |  | N2 | O2 | HCL
1) Idle state |  | 850 | 3 | 0 | 0
2) Push wafer into furnace | 5 | 850 | 3 | 0 | 0
3) Ramp up temp. | 15 | 10°C/min | 3 | 0 | 0
4) Temp. stabilization | 5 | 1000 | 3 | 0 | 0
5) Dry oxide growth | 30 | 1000 | 0 | 2.5 | .067
6) Anneal | 30 | 1000 | 3 | 0 | 0
7) Ramp down temp. | 75 | -2°C/min | 3 | 0 | 0
8) Retrieve wafer | 850 | 3 | 0 | 0 | 

## Slide 29: Ramping
With any furnace process, temperatures need to be changed slowly when wafers are present.
The ramp-up rate (in this recipe) is 10oC/min. The ramp-down rate is –2oC/min.
These slow rates are necessary to prevent warping or other thermal stress problems in the silicon wafers.

## Slide 30: Dry Ox. Growth Rate
5000
4000
3000
2000
1000
100
200
300
400
500
Time (min)
Oxide Thickness (Å)
Approximately linear growth region
Public Domain: Image generated by CNEU Staff for free use

## Slide 31: Outline
Introduction – Silicon dioxide
Types of Oxide
Furnace Deposition
  Dry Oxidation
  Wet Oxidation
High Pressure Oxidation
Chemical Vapor Deposition
Modifying Dielectric Constant

## Slide 32: Wet Oxidation
Oxidation that occurs as a result of steam reacting with silicon
  Si + 2H2O  SiO2 + 2H2
Grows oxide at a much faster rate and produces a lower quality oxide
Use this technique when very thick oxides (i.e. field oxide) are needed rather than high quality

## Slide 33: Wet Oxidation
The process is performed in the furnace at high temperatures (normally 1000oC)
Uses steam as the process gas
  Steam is pyrolytic meaning that in high heat H2 and O2 are reacted together to create water vapor molecules
  This produces a much purer steam for oxidation

## Slide 34: Chlorinated Agents
  Using chlorinated gases in the oxidation process can neutralize charge accumulation at the silicon oxide interface.
  Chlorinated agents are kept under 3% so instability is not created in the oxide layer.
  Chlorinate agents can increase growth rates by 10-15%. This mechanism is poorly understood.
  Trichloroethane (TCA), an organochloride, offers low corrosion to the oxidation system.

## Slide 35: Wet Ox. Growth Rate

## Slide 36: Wet Vs. Dry Oxidation
Dry Ox. Grows higher quality oxides
  In Wet Ox., steam reacts with silicon and produces hydrogen molecules. These molecules become trapped in the oxide and change the stoichiometry of the oxide
    Stoichiometry indicates how closely the deposited film approaches the ratio of the elements given by its chemical formula

## Slide 37: Wet Vs. Dry Oxidation
Wet Ox. grows oxides faster
  At 1000oC, the solubility of water in silicon (total amount of water that can be present in a certain volume of silicon) is 600 times that of oxygen in silicon.
  Even though oxygen diffuses faster, it has a lower solubility and physically can fit fewer atoms in the silicon.

## Slide 38: Wet Vs. Dry Oxidation
Oxide Type | Temp (°C) | Thickness (Å) | Time
Dry | 1000 | 1000 | 2 hours
Wet | 1000 | 1000 | 12 minutes

## Slide 39: Wet and Dry Oxide Growth
Oxide Thickness (µm)
Time (hours)

## Slide 40: Increasing Temp. – Decreasing Time
There are many problems with increasing the temperature at which a process runs.
  Increased diffusion of impurities present in the wafer
  Crystal defects (stacking faults)
  Permanent damage from thermal stress
  Equipment damage/more costly equipment to run at higher temperatures

## Slide 41: Outline
Introduction – Silicon dioxide
Types of Oxide
Furnace Deposition
  Dry Oxidation
  Wet Oxidation
High Pressure Oxidation
Chemical Vapor Deposition
Modifying Dielectric Constant

## Slide 42: High Pressure Oxidation - HiPOx
Used to grow thick layers of oxide in reduced time and temperature (i.e. field oxide)
Uses steam and oxygen as process gases
Has special HiPOx system equipment

## Slide 43: HiPOx System
Quartz Tube
Breech
Door
End Cap
Heating Element
Injector Baffle
Injector-
Steam
Public Domain: Image generated by CNEU Staff for free use

## Slide 44: HiPOx
Runs at reduced temperatures:
  ~ 650oC – 900oC
And increased pressures:
  ~ 5 – 20 atm.

## Slide 45: HiPOx Relationships
Time and pressure are inversely related:
*Assuming that the wafers are of the same thickness
Temp. (°C) | Pressure (atm.) | Time
900 | 1 | 5 hours
900 | 5 | 1 hour
900 | 25 | 12 minutes

## Slide 46: HiPOx Relationships
Temperature and Pressure:
  For every increase of one atmosphere, the temperature can be dropped by 30oC to obtain the same thickness in the same time
Time (hours) | Pressure (atm.) | Temp. (°C)
5 | 1 | 1000
5 | 10 | 700

## Slide 47: HiPOx Relationships
Temperature and oxide density:
  As temperature decreases, oxide density increases.

## Slide 48: HiPOx
HiPOx allows the oxidation to occur at a lower temperature and higher pressure.
As shown, HiPOx will produce a higher quality (greater density) oxide in a shorter time than dry or wet oxidation can produce (for equal thickness).

## Slide 49: Outline
Introduction – Silicon dioxide
Types of Oxide
Furnace Deposition
  Dry Oxidation
  Wet Oxidation
High Pressure Oxidation
Chemical Vapor Deposition
Modifying Dielectric Constant

## Slide 50: CVD
The deposition of oxide onto a wafer using the decomposition of silane.
  SiH4 + O2  SiO2 + 2H2
“Deposits” a layer of oxide as opposed to the other techniques that “grow” the oxide.

## Slide 51: CVD
Oxide is deposited at ~ 350oC.
Silicon and oxygen react in plasma and deposit onto the wafer (other techniques diffuse O2 into the wafer and use the wafer’s silicon to produce oxide)
Creates a nearly stoichiometric layer

## Slide 52: Index of Refraction
SiO2
n=1.46
Air
n=1.0

Air
n=1.0
SiO2
n=1.46

Public Domain: Image generated by CNEU Staff for free use

## Slide 53: CVD
Nitrous oxide (N2O) or carbon dioxide (CO2) are actually preferred over oxygen.
The oxygen reacts too easily in the plasma and can cause poor film quality.

## Slide 54
Outline
Introduction – Silicon dioxide
Types of Oxide
Furnace Deposition
  Dry Oxidation
  Wet Oxidation
High Pressure Oxidation
Chemical Vapor Deposition
Modifying Dielectric Constant

## Slide 55: Engineering Dielectric Constant (k)
This concept centers around capacitance (C) and its relationship to signal time (T) when fabricating integrated circuits
k= dielectric constant
 o= permittivity of free space (constant)
A= area
d= distance between features
C =ko A
d

## Slide 56: Engineering Dielectric Constant (k)
Signal Time (T)
R= resistance of metals
C= capacitance
In IC fabrication, the idea is to use the correct dielectric material with the right constants for a desired process
  Keeps the capacitance the same to insure the signal time is not compromised
T= RC

## Slide 57: Engineering Dielectric Constant (k)
Figure of Merit
  The figure of merit is a number expressed in farads/meter and is calculated by dividing capacitance (C) by area (A)
  Used as a constant in IC fabrication
  If device scaling changes, the dielectric material must change to maintain the figure of merit’s value
C/A = figure of merit

## Slide 58: Engineering Dielectric Constant (k)
Interconnects- wiring
  The wire lines must be as close as possible in order to fit the maximum amount of transistors on a chip
  The distance must be minimized, therefore; the dielectric material must have a low k
  As d decreases, k must also decrease

## Slide 59: Engineering Dielectric Constant (k)
Gates
  Uniformity is a key quality parameter
  It is easier to make the gates thicker, to insure that any variation in uniformity won’t impact device performance as drastically
  Example 1: If a gate is 30Å:
    Material uniformity that varies by 10Å drastically alters performance
  Example 2: If a gate is 100Å
    Material uniformity that varies by 10Å does not impact performance that drastically

## Slide 60: Engineering Dielectric Constant (k)
Gates
  A thicker gate requires a dielectric material with a high k value
  As d increases, k must also increase

## Slide 61: High k Dielectric Materials
Ta2O5, k = 22-30
TiO2, k = 20-85
Nb2O5, k = 11
HfO2, k = 17
Y2O3, k = 15

## Slide 62: Low k Dielectric Materials
FSG, k = 3.4-4.1
HSQ, k = 2.9
Nanoporous silica, k = 1.3-2.5
Fluorinated polyimide, k = 2.6-2.9
PTFE, k = 1.9
DVS-BCB, k = 2.65
Aromatic hydrocarbon, k = 2.65