Microfluidics

Objective:  The students will gain knowledge and experience creating microfluidic devices.  This lab will use negative lithography to create a master mold for PDMS microfluidic structures.  Application, curing, and adhesion of the PDMS to glass will be covered.

Background:  Microfluidics is a broad term used to describe different applications of fluid transport through channels and networks in the micron regime.  A microfluidic channel is typically defined as a channel having one or more dimensions less than 100 microns in size.  The transport mechanisms by which liquids are transferred include capillary forces, hydrostatic pressure gradients, electrokinetics, pumps, magnetism, and digital arrays.  Even more novel ways to move fluids are being created, with material selection an important aspect to consider when deciding on the transport mechanism.  Some of the earliest recorded electrokinetic microfluidic studies utilized silicon substrates but the expense and need for insulating the surface has shifted the focus to plastics and glass.  In this lab, we will describe the fabrication issues involved with these devices and show the application of hydrostatic transport of a liquid media.

Figure I.  An example of a microfluidic channel.

Equipment/Training Required:  Photolithography training, Karl Suss MJB3, Optical Microscope.

Process: Overview Day 1

- Perform negative lithography on a silicon substrate to create master mold

- Inspect the quality of the lithography with the optical microscope

- Determine the channel dimensions with the profilometer.

- Pour PDMS over the mold and cure at 65 oC for 3 hrs

- Remove cured PDMS from a previously made master mold

- Punch the PDMS with a needle to create access points to the channels

- Use isopropanol in the sonic cleaner to clean the glass substrate and the PDMS for 3 min

- Dry with nitrogen (Do not perform a DI water rinse)

- Activate the surface of the PDMS and the glass substrate with the surface activator

- Apply PDMS with channels to glass substrate and allow the bonding to occur overnight.

Process: Overview Day 2

- Glue needles to the inlets of a pre-bound PDMS/glass substrate using epoxy.

- Fill the microfluidic channels

- Image the fluid flow with microscope

Negative Lithography Procedure:  Creation of Master Mold

- Clean a silicon substrate with acetone, IPA, and DI water

- Dehydration bake for 3-4min at 105°C

- HMDS application

- Dehydration bake for 15sec at 110°C

- Spin on SU8-25 photoresist for a thickness of approximately 25µm

  - Use recipes SU25.20/30

    - The first step of each recipe is 25 seconds at 500 RPM

    - The second step is 2000 RPM for 35 seconds

  - Note: Use an 8mL pipette and cut the tip down to facilitate application of photoresist.

- Perform a two step soft bake.

  - Soft bake for 3min @ 65°C

  - Soft bake again for 7min @ 95°C

- NOTE:  Do not use the cooling chuck between bakes.  This will minimize the thermal stress on the film

- Expose to UV light in the MA/BA6 for 20 seconds using the microfluidic channel mask

- Perform a two step post-exposure bake.

  - Post exposure bake for 1min @ 65°C

  - Post exposure bake again for 3min @ 95°C

- Develop in SU-8 developer.

  - Bath 1 for 2min

  - Bath 2 for 2min

  - Bath 3 for 1min

  - Additional development may be needed in the 3rd bath

- Rinse and dry the sample

Questions:

- Name three reasons PDMS is used for microfluidic devices?  (3)

- Explain how the photoresist was used in this lab.  (3)

- Compare the channel dimensions of the mask to the channel dimensions achieved after photolithography.  Give reasons for any variations. (3)

- Define the following mechanisms for fluid transport in a microfluidic system. (4)

  - Hydrostatic

  - Capillary

  - Electrophoresis

  - Electro-osmosis

- Acquire and read a copy of the following article and answer theses questions.

S. Bhattacharya et al. Studies on Surface Wettability of Poly(Dimethyl) Siloxane (PDMS) and Glass Under Oxygen-Plasma treatment and Correlation With Bond Strength.  Journal of Microelectromechanical Systems. Vol. 14, No. 3, June 2005

  - What are the two competing schools of thought behind the mechanisms of oxygen plasma treatment and PDMS bonding? (4)

  - How did the chemical treatment of the glass substrate and the PDMS affect the bonding of the two materials? (2)

  - In the RIE, how was the bond strength affected when chamber pressure was increased? (2)

  - What was the maximum bond strength found to be for glass to PDMS found to be? (2)

  - What is the universal trend in the relationship between glass to PDMS bonding and contact angle?  (2)

- Research and submit one reference on a microfluidic application and give a brief    summary of the project and results. (5)

Lab reports are due 12:00 NOON the Monday following the lab completion date.

NO WORK WILL BE ACCEPTED LATE!