## Slide 1
Focused Ion Beam (FIB): “Seeing” and “Processing” at the Nano-Scale

## Slide 2
Outline
FIB Overview
FIB Operation
FIB Applications

## Slide 3
FIB overview

## Slide 4
Beam Interactions
Note difference in interaction volume
Milling as it scans sample surface
No damage as it scans sample surface
Ebeam vs. Ion Beam

## Slide 5
Ion beam lithography
Image Analysis
Film Deposition
Ion Milling (Dry Etching)
Applications of Focused Ion Beam (FIB)

## Slide 6
Electron Column
Ion Column
Vacuum Chamber
Door
Typical Configuration of FIB

## Slide 7: FEI Quanta 3D system
Pt Gas Injection System (GIS)
Electron Column
Ion column (Ion pump showing)
Stage motors
Typical Configuration of FIB (continued)

## Slide 8: FEI Quanta 3D system
Omniprobe
Tungsten Gas Injection System (GIS)
Typical Configuration of FIB (continued)

## Slide 9: FEI Quanta 3D system
BSD
Sample stage
Ion Column
GIS (Pt)
SEM Column
Typical Configuration of FIB (continued): 0 degree tilted

## Slide 10
Typical Configuration of FIB (continued): 52 degree tilted

## Slide 11
Typical Configuration of FIB (continued): User Interface

## Slide 12
Typical Configuration of FIB (continued): User Interface

## Slide 13
FIB operation

## Slide 14: All equipment is pointed to one central spot !!
E-beam
Ion-beam
Eucentric height =15mm WD below e-column pole piece and 30mm from I column
GIS
What is Eucentric Point ?

## Slide 15
All aligned:
  “Eucentric” is a point in the stage height control (“Z”) where the sample’s image does not move when the sample is tilted.
  SEM imaging is used to find the physical point.
Tilt Plane
IMAGE
15 mm SEM WD
What is Eucentric Point ? (continued)

## Slide 16
SEM:Imaging
FIB: Cutting
52°
52°
38°
Eucentric Point (continued)

## Slide 17
Ion mage - Appears to be looking straight on.
SE image is foreshortened. The upper part of the image is at a longer WD than the lower portion of the image.
Eucentric Point (continued) – 52 degree tilted Images

## Slide 18
Ion image is doing the cutting and “looking” down in the sample.
SE image can look into the milled area.
Eucentric Point (continued) – 52 degree tilted Images

## Slide 19
“Eucentric” is the point on the height of the stage in which the sample stays centered as the stage is tilted.
It’s assumed you are at about 15 mm WD (having done a Z<>FWD and moved the stage previously)
Only after finding the eucentric point, you have coincidence alignment of the beams!
Eucentric Point Finding Steps

## Slide 20
You will perform the following steps in the upcoming slides:
  Start at ‘0’ degrees tilt
  Note a feature of interest and bring to a feature of interest (e.g., center of crosshairs)
  Tilt the stage to a positive 52 degrees
  Watch the image move either up or down on the screen
  Adjust the “Z” height on the specimen door to bring feature back to the center of the screen
  You may have to do this several times at higher and higher magnifications to get perfect eucentricity
Eucentric Point Finding Steps (continued)

## Slide 21
Fine Alignment of Ion Beam

## Slide 22
E-Beam
Ion-Beam
We just set up the sample to face the Ion beam

## Slide 23
The ion beam will damage your sample when viewing. It is important to use a small beam size when imaging!
When getting ready to mill with a large beam current, you must focus quickly and in as few of scans as possible!
While milling or depositing a film, you can highlight Quad 1 (SE column) and take a photo (F2) or click “snapshot.” or. It will pause the Ion beam and grab a quick SE image to see status of the Ion milling operation.
Ion Beam Operation

## Slide 24
Pt. deposition can be used for many applications.
  adding a conductive layer to a non conductive sample
  setting up a pattern, to prevent “curtaining” with the FIB
  adhesive attachment for mechanical testing
  - This tutorial will cover the second point: making a protective shield for further processing
Film Deposition (Pt)

## Slide 25
Ion Beam
Gas Injection System
Film Deposition (Pt)-continued
Notes: The gas is delivered through a needle very close to sample. This needle is usually retracted out of the way until needed.
It is pre-adjusted to be about 100 microns above the sample, and about 100 microns away from the center of the scan.
Having the needle reasonably close allows a smaller volume of gas and this is easier on the pump and chamber.

## Slide 26
Click on the third Icon - the Patterning Page
This page controls:
Patterning type including size
Progress of mill or deposition
Gas injection
End Point Monitor
Film Deposition (Pt)- Find Deposition Spot

## Slide 27
Double click “cold” to toggle on “warm”
-This heats the Pt. Gas deposition system.
Film Deposition (Pt)-Warm up the Pt Source

## Slide 28
Click on click box under “In”, to inject the GIS needle
Check Quad 4 to see that the needle appears to be inserted properly
Film Deposition (Pt)-Insert Pt Gas Injector

## Slide 29
Select “Rectangle”.
Draw a rectangle on the frozen Ion image by clicking and dragging the left mouse button.
Make the rectangle about 10 X 1 X 1 Micron in X,Y, and Z values.
Increase mag so rectangle fills large fraction of screen
Verify “Pt dep” is selected as application on the “basic” tab
Film Deposition (Pt)-Define the Deposition Area

## Slide 30
Set Ion current to 0.10 nA for dep.
Un Pause and quickly focus, if a “Beam Shift” is necessary, move image so that it is still aligned to SEM image.
Re-alignment of the deposition pattern box may also be necessary.
Film Deposition (Pt)- Deposition Condition Setup

## Slide 31
Start the Dep by clicking the “Start” icon
Note the various parameters in Pattern menu. These will become more important to you later, but its good to get exposed now, while you are waiting for a deposition.
Film Deposition (Pt)-Start Deposition

## Slide 32
You may take a quick peak at the depositions, as it progresses by using the “Snapshot” feature.
- Enable Quad 1
- Click on the “SnapShot” icon
Film Deposition (Pt)- Deposition Progress Check

## Slide 33
Film Deposition (Pt)- Images of Deposited Film
Electron beam image
Ion beam image

## Slide 34
Metal deposition
SEM
FIB
Sample plane
Cross section
Projection of sample plane to SEM image plane
Projection of cross section plane to SEM plane
Cross section image surface
Stage at 0°
Cos 52°
SEM:Imaging
FIB: Cutting
52°
Sin 52°
52°
38° from 0°
38°
Key
Ion Milling

## Slide 35
Start with “Regular Cross Section”
Click and draw a rectangular box on the prepared sample
Align the rectangle just below the Pt.dep area
Set “Application” to “Si”, as default cutting parameters
Ion Milling: Basic Step

## Slide 36
Increase the ion beam current to 5 nA
Quickly scan and focus (you are milling as you scan)
Pause as soon as the image is in focus
Re-align the milling pattern if necessary on the frozen image
Ion Milling: Ion Beam Setup

## Slide 37
Verify that the rough cross section is 10 X 4.5 X 4 microns deep and aligned just touching the Pt. Dep pattern.
Start Milling
If you have a BSD, you may image live in Quad 3 as the sample is milled.
Ion Milling: Milling

## Slide 38
Milling has now started
Note time remaining
Take a break for that time period (tell your boss its an order)
If you are curious, click on Quad 1 and then “snapshot”. That will give you a quick SE image of your milling progress
Ion Milling: Progress Check

## Slide 39
View the rough cut with the SEM
Click on Quad 2 and adjust ion beam current to 0.3 nA
Select “cleaning cross section” pattern
Scan and focus with the ion beam and then pause
Redraw a smaller pattern on the frozen ion beam image
Use a depth 1/3rd that of the regular cross section
Start milling
Ion Milling: Cleaning Cut

## Slide 40
View the rough cut with the SEM
Click on Quad 2 and adjust ion beam current down to 50 pA
Select “cleaning cross section”
Scan and focus with the ion beam and then pause
Redraw a smaller pattern on the frozen ion beam image
Start milling
Ion Milling: Cleaning Cut

## Slide 41
Ion Milling: SEM Image of the Cut

## Slide 42
http://www.fibics.com/fib/tutorials/Grain-Orientation-Contrast/6/
FIB is more than four times as intense as that produced by backscattered electrons in the SEM, and results in spectacular grain contrast, as can easily be seen in the FIB image of aluminum grains in the image.
FIB Grain Contrast

## Slide 43
FIB Grain Images: W filament

## Slide 44
FIB Applications

## Slide 45
Electrode Formation for Nanowires
Y. Long et. al, Appl. Phys. Lett. (2003)

## Slide 46
Cross Sectional TEM Sample Preparation
http://www.pdx.edu/cemn/fib-gallery