## Slide 1
Introduction to Nanotechnology
Module #4
The Uniqueness of the Nano-scale
Nanotechnology is Impacting Everything
© patton brothers illustration (www.pattonbros.com)
Copyright April 2009 The Pennsylvania State University
Last Updated: 1/6/2011
Notes: <number>
There is a glossary that comes along with this set of modules. Each term in blue print in every module is defined in this glossary.

## Slide 2
  This module is one of a series designed to be used by faculty members at post-secondary institutions in workshops, courses, and overview lectures to introduce nanotechnology and its applications. There is no particular significance to the module number system
  The series was funded in part by:
  The National Science Foundation
  Grant # DUE 0532646
  and
  The Pennsylvania Department of Community and Economic Development
  Grant # C000029471
  Any opinions, findings, and conclusions or recommendations expressed in this material are those of the author and do not necessarily reflect the views of the National Science Foundation or the Pennsylvania Department of Community and Economic Development
Copyright April 2009 The Pennsylvania State University

## Slide 3: Glossary of Terms
Throughout these modules you will find words and terms printed in the color blue. These words and terms are defined in the glossary (glossary.html), which can be opened by clicking here.
Copyright April 2009 The Pennsylvania State University

## Slide 4
As we’ll see, new doors open at the nano-scale:
  New things happen and new opportunities become accessible
“It is Sometimes Better to be Little”
Copyright April 2009 The Pennsylvania State University

## Slide 5: Outline
A listing of some of the unique attributes of the nano-scale
Some examples of the impact of these unique attributes
Key Ideas
Copyright April 2009 The Pennsylvania State University

## Slide 6: Outline
A listing of some of the unique attributes of the nano-scale
Some examples of the impact of these unique attributes
Key Ideas
Copyright April 2009 The Pennsylvania State University

## Slide 7: Here is a Listing of Some of the Unique Attributes of the Nano-scale
Very small size—obvious yet the impact is tremendous!
High surface to volume ratio ─ resulting in many, if not most, of the atoms being on the surface
High surface to volume ratio ─ resulting in a unique surface environment for most of the atoms
Surface forces dominate over bulk forces ─ for example, gravity (a bulk force) is not important
Quantum mechanical effects are important
Wave properties of light are important
Copyright April 2009 The Pennsylvania State University

## Slide 8: Some of the Unique Attributes of the Nano-scale (continued)
Sizes corresponding to basic biological structures
Sizes corresponding to macro-molecules
Unique chemical bonding configurations possible
Size range in which molecules can self-assemble
New epistemologies (Working at the nano-scale has caused us to learn new ways of “seeing” our world)
Copyright April 2009 The Pennsylvania State University

## Slide 9: Outline
A listing of some of the unique attributes of the nano-scale
Some examples of the impact of these unique attributes
Key Ideas
Copyright April 2009 The Pennsylvania State University

## Slide 10
Very Small Size
R (radius)
Can fit many “nano-sized things” together with little space in between
Can get large number of “nano-sized things” per volume
Or, can get large number per area
Copyright April 2009 The Pennsylvania State University

## Slide 11
An example of an impact of this attribute: Huge Areal Densities
The huge number of nano-scale transistors possible per area means today’s state-of-the-art microelectronics circuits with their nano-scale transistors can give more speed and more functionality.
Copyright April 2009 The Pennsylvania State University
Mick Feuerbacher, December 2005.
Copyright Matco Services Inc. www.materialsforum.com
Notes: <number>

## Slide 12
High surface to volume ratio
R
Ratio = 3/R
This ratio is very big when R is very small
Ratio =
4πR2_
4/3πR3
Copyright April 2009 The Pennsylvania State University

## Slide 13: Impact of the Huge Surface to Volume Ratio
Percent Surface Atoms
Diameter (nm)
This figure shows the inverse relationship between particle size and number of surface atoms.
As a particle gets smaller, a larger and larger percentage of the atoms that make up the particle
are surface atoms.
Because the number of atoms or molecules on the surface of a particle influences the particle’s
chemical and physical interactions with its environment, this percentage in the figure is key to
defining the chemical and biological properties of nanoparticles.
Figure 1 from Andre Nel, Tian Xia, Lutz Mädler and Ning Li., SCIENCE Vol.311. p. 622 (2006).
Copyright April 2009 The Pennsylvania State University

## Slide 14
Reprinted figure with permission from Buffat and Borel, “Phys Rev. A” Volume 13, p 2287 (1976). Copyright 1976 by the American Physical Society.
An example of an impact of this attribute: Melting Temperature
This data
is for Gold
The melting temperature gets lower as a nanoparticle gets smaller because higher percentage of atoms are on the surface. This makes sense since surface atoms are not bound to each other the same way bulk atoms are.
Particle diameter in Angstroms
Copyright April 2009 The Pennsylvania State University

## Slide 15: Surface Forces Dominate over Bulk Forces
Bulk force importance decreases with decreasing volume
Surface force importance increases with decreasing volume
Copyright April 2009 The Pennsylvania State University

## Slide 16: Surface Forces Dominate over Gravity
Gravity’s importance decreases with decreasing volume
Surface force importance increases with decreasing volume
gravity
gravity
Surface
forces
Copyright April 2009 The Pennsylvania State University

## Slide 17: An example of an impact of this attribute: Colloidal Solutions
The nano-scale colloidal particles in the solutions seen above will never settle out. (so long as surface forces are not present to cause them to agglomerate. If they agglomerated, this would increase particle volume and give gravity a chance to become important)
Copyright April 2009 The Pennsylvania State University
“Electronic Imaging & Signal Processing: Improving biomedical imaging with gold nanocages” by Younan Xia and Sara E. Skrabalak. 12 May 2008, SPIE Newsroom. DOI: 10.1117/2.1200705.1135

## Slide 18: Emergence of Quantum Mechanical Effects
Electrons can only have certain energies in atoms due to quantum mechanics.
Semiconductor nanoparticles can behave like man-made atoms and have only certain energies allowed for electrons.
The energy difference between these allowed energies in nanoparticles gets bigger as R gets smaller
R
Copyright April 2009 The Pennsylvania State University
Notes: <number>
Bigger energy differences between allowed energies as R gets smaller means larger energy photons are emitted when electrons relax from the higher (excited) energy band to the lower (ground state) energy band. Higher energy photons means shorter wavelength light.

## Slide 19: An example of an impact of this attribute: Semiconductor Quantum Dots When excited by light, quantum dots fluoresce (re-emit light). The size and material composition of nano-scale quantum dots dictates the color they re-emit.
Copyright April 2009 The Pennsylvania State University
Evidenttech.com

## Slide 20: Importance of the Wave Properties of Light
The wavelength  of visible light is much larger than the sizes R of nano-scale structures.
Because of this, light scatters and diffracts when it interacts with nanostructures
Copyright April 2009 The Pennsylvania State University

## Slide 21: An example of an impact of this attribute: Photonic Crystals Man-made nano-structures can cause light to turn sharp 90 degree corners, as seen below
Copyright April 2009 The Pennsylvania State University
Reproduced with permission of the MRS Bulletin. www.mrs.org/bulletin

## Slide 22: Butterfly Scales
20,000 x magnification
5000x magnification
220x magnification
1x magnification
of wing
Another example of an impact of this
attribute
Nanostructures can cause light of different colors to scatter and
diffract differently. This effect is used by nature to give the colors
seen in butterfly wings.
Militaries Study Animals for Cutting-Edge Camouflage. James Owen in England for National Geographic News March 12, 2003, Proc. R. Soc. Lond. B (1999) 266, 1403-1411
Copyright April 2009 The Pennsylvania State University
Notes: <number>
We have already seen that Nature has a number of ways to create colors. In these modules we have so far seen (1) metal nanoparticle plasmom behavior which gives rise to color, (2) single electron transitions in semiconductor nanoparticles which gives rise to color, and now (3) geometric interference effects which also can give rise to color.

## Slide 23: Sizes Corresponding to Basic Biological Structures
We can now easily make structures in the 1nm to ~100nm size range.
This is the size range of many of the key structures in biological systems
Copyright April 2009 The Pennsylvania State University

## Slide 24
The cell is a complex structure with many compartments and organelles possessing individual and interdependent functions. Many of a cell`s features (e.g., pores) and, of course, DNA and RNA are all in the nano-scale. We can now make structures like these smallest of features in a cell.
An example of an impact of this attribute:
Copyright April 2009 The Pennsylvania State University
Public Library of Science, “The Intersection of Biology and Materials Science” by George M. Whitesides and Amy P. Wong Vol. 31, p. 23.

## Slide 25
Golovchenko, Branton, et. al. (Harvard Nanopore Group)
Sequencing DNA using nanopore ionic conductance.
Another Example: Structures that can “read” DNA
Can now make structures so small that they, for example, can force DNA to line-up single file in order to pass through
We can now use electrical signal changes to “read” the DNA as it passes through
DNA
Copyright April 2009 The Pennsylvania State University

## Slide 26
DNA: millions of atoms long but 2.5 nm wide
Nanostructures can have the dimensions seen in macromolecules
Copyright April 2009 The Pennsylvania State University
The Chaim Weizmann Institute of Chemistry, and the Fritz Haber Research Center for Molecular Dynamics, The Hebrew University of Jerusalem.

## Slide 27
We can now make man-made versions of Nature`s motors like this one. Here Myosin V (blue), a cellular motor protein, carries cargo within cells by moving along actin filaments (red). It takes 37 nanometer steps by placing one “foot” over the other, as revealed by a fluorophore tag (rainbow-colored oval).
[Illustration: PrecisionGraphics.com]
Ahmet Yildiz, Joseph N. Forkey, Sean A. McKinney, Taekjip Ha, Yale E. Goldman, Paul R. Selvin: Myosin V Walks Hand-Over-Hand: Single Fluorophore Imaging with 1.5-nm Localization. Science. 2003. Vol. 300. p.2061
An example of an impact of this attribute:
Copyright April 2009 The Pennsylvania State University

## Slide 28
Unique chemical bonding configurations possible
Carbon nanotubes
Copyright April 2009 The Pennsylvania State University
Odom et al, J. Phys. Chem. B104, 2794 (2000). Copyright Wiley-VCH Verlag GmbH & Co. KGaA. Reproduced with permission.

## Slide 29: An example of an impact of this attribute Superior strength concrete for construction made with CNTs
Carbon nanotubes distributed on small cement grains
Copyright April 2009 The Pennsylvania State University
S Bulletin, Vol. 31. P. 23, January 2006 Makar, J. M Beaudoin, J.J/NRCC-46618 http://irc.nrc-cnrc.gc.ca/ircpubs. Reproduced with the permission of the Minister of Public Works and Government Services Canada, 2009.
Notes: <number>
CNTs = carbon nanotubes

## Slide 30
Molecular Self-Assembly
An example: a mixture of two polymeric molecules can be made to self-assemble, under the influence of heat, into a structure with one phase made up only of molecules of type 1 and another phase made up only of molecules of type 2
White phase (regions) is made
up only of molecules of type 1
Black phase (regions) is made up
only of molecules of type 2
Copyright April 2009 The Pennsylvania State University
Courtesy of CNEU

## Slide 31
New Ways of Seeing things
The nano-scale tips on scanning probe
microscopes (SPMs) allow us to even “see” atoms
Actual Atoms!
IBM Research Division
M.F. Crommie, C.P. Lutz, D.M. Eigler. Confinement of electrons to quantum corrals on a metal surface. Science 262, 218-220 (1993).
Copyright April 2009 The Pennsylvania State University

## Slide 32: Examples of the impact of this attribute: New tools for “seeing”
Electron beam-based techniques
TEM (Transmission Electron Microscopy)
SEM (Scanning Electron Microscopy)
Nano-scale-sized probe-based scanning techniques
AFM (Atomic Force Microscopy)
STM (Scanning Tunneling Microscopy)
NSOM (Near Field Optical Microscopy)
Copyright April 2009 The Pennsylvania State University
Courtesy of Evans Analytical Group®
Notes: <number>
Tools and the size range they can “see” at

## Slide 33: Outline
A listing of some of the unique attributes of the nano-scale
Some examples of the impact of these unique attributes
Key Ideas
Copyright April 2009 The Pennsylvania State University

## Slide 34: Key Points
Nanostructures are extremely small – so small that gravity is not an important force in the nano-scale world
Nanostructures have large surface to volume ratios which affect properties from their chemical activity to their melting temperature
Copyright April 2009 The Pennsylvania State University

## Slide 35: Key Points (Continued)
3. Nanostructures are so small that quantum mechanical phenomena can become very apparent
4. Nanostructures are so small that phenomena resulting from the wave properties of light (physical optics) can become very apparent
5. Nanostructures are so small that they can have unique chemical bonding
Copyright April 2009 The Pennsylvania State University

## Slide 36: Key Points (Continued)
6. Nanostructures are so small that their size corresponds to that of macro-molecules
7. Nanostructures are so small that their size corresponds to that of basic structures in biology
8. Nanotechnology has provided us with new tools to see the universe we live in—it has given us new epistemologies.
Copyright April 2009 The Pennsylvania State University

## Slide 37
This module, produced by the Center for Nanotechnology Education and Utilization at
The Pennsylvania State University,
is one of a series developed to introduce nanotechnology and its applications to a broad audience. Each module, its component viewgraphs, and the companion glossary are copyrighted 2009 by
The Pennsylvania State University.
All rights reserved.
Copyright April 2009 The Pennsylvania State University