## Slide 1
Introduction to Nanotechnology
Module #5
How Do We “See” Things at the Nano-scale:
An Introduction to Characterization Techniques
Nanotechnology is Impacting Everything
© patton brothers illustration (www.pattonbros.com)
Copyright April 2009 The Pennsylvania State University
Last Updated: 1/6/2011
Notes: <number>
There is a glossary that comes along with this set of modules. Each term in blue print in every module is defined in this glossary.

## Slide 2
  This module is one of a series designed to be used by faculty members at post-secondary institutions in workshops, courses, and overview lectures to introduce nanotechnology and its applications. There is no particular significance to the module number system
  The series was funded in part by:
  The National Science Foundation
  Grant # DUE 0532646 and DUE 0802498
  and
  The Pennsylvania Department of Community and Economic Development
  Grant # C000029471 and C000036659
  Any opinions, findings, and conclusions or recommendations expressed in this material are those of the author and do not necessarily reflect the views of the National Science Foundation or the Pennsylvania Department of Community and Economic Development
Copyright April 2009 The Pennsylvania State University

## Slide 3: Glossary of Terms
Throughout these modules you will find words and terms printed in the color blue. These words and terms are defined in the glossary (glossary.html), which can be opened by clicking here.
Copyright April 2009 The Pennsylvania State University

## Slide 4: Outline
What do we mean by “seeing” at the nano-scale
Electron beam-based tools for producing images using electrons
Electron beam-based tools for producing composition information using x-ray photons
Scanning probe tools
How small can we go?
Key Ideas
Copyright April 2009 The Pennsylvania State University

## Slide 5: Outline
What do we mean by “seeing” at the nano-scale
Electron beam-based tools for producing images using electrons
Electron beam-based tools for producing composition information using x-ray photons
Scanning probe tools
How small can we go?
Key Ideas
Copyright April 2009 The Pennsylvania State University

## Slide 6: “Seeing” at the Nano-scale
By “seeing” at the nano-scale, we mean (1) being able to literally see size, shape, and structure, (2) being able to determine the composition ( i.e., the elements present), and (3) being able to determine physical and chemical properties of the tiny, tiny structures used in nanotechnology. Engineers and scientists give this “seeing”, which may be done with the help of electrons, ions, photons, or scanning probes, the name “characterization”.
Copyright April 2009 The Pennsylvania State University
Notes: <number>

## Slide 7: Outline
What do we mean by “seeing” at the nano-scale
Electron beam-based tools for producing images using electrons
Electron beam-based tools for producing composition information using x-ray photons
Scanning probe tools
How small can we go?
Key Ideas
Copyright April 2009 The Pennsylvania State University

## Slide 8: Seeing at the Nano-scale
One way to see things at the nano-scale is to use beams of electrons.
These beams can be used to let us see size, shape, structure and even composition.
Copyright April 2009 The Pennsylvania State University
Notes: <number>

## Slide 9: A Beam of Electrons Interacts in Many Ways when it Impinges on a Material
When a beam of electrons hits a material (specimen), a number of responses occur. Some of the electrons may go through the specimen (transmitted electrons). Some may bounce back (backscattered electrons) and new electrons may be knocked off the atoms of the specimen and come back out (secondary electrons and Auger electrons). In addition, photons, including high energy photons (x-rays), generated by the relaxing of excited atoms may come back out.
Each one of these responses can be exploited to “see” the specimen
14 Jan. 2009 by F. Krumeich. © ETH Zürich and the authors
Copyright April 2009 The Pennsylvania State University
Notes: <number>
The incident beam originates at a source. The electron source is heated to boil-off the electrons (thermionic emission) or it is designed so that the electrons can quantum mechanically tunnel out. The latter is called a field emission (an old name for tunneling) source and it is better because the electrons are more mono-energetic and therefore easier to manipulate to get better images. The electrons that come from a thermal emission source have a variety of energies because they have picked up some thermal energy and are therefore harder to manipulate..

## Slide 10: Using the Transmitted Electrons to “See”
Seeing by using the transmitted electrons is called transmission electron microscopy (TEM). It is called field emission transmission electron microscopy (FE-TEM) when the impinging beam of electrons is produced by quantum mechanical tunneling.
Copyright April 2009 The Pennsylvania State University
Notes: <number>

## Slide 11: Schematic of a TEM or FE-TEM
JEOL 2010F
Semiconductor Material and Device Characterization, 3rd ed. Dieter K. Schroder, John Wiley & Sons, Inc. p 647. 1999
Copyright April 2009 The Pennsylvania State University
Notes: <number>
The electron source is heated to boil-off the electrons (thermionic emission) or it is designed so that the electrons can tunnel out. The latter is called a field emission (an old name for tunneling) source and it is better because the electrons are more mono-energetic.The electrons that come from a thermal emission source have a variety of energies because they have picked up some thermal energy. When an electron beam from the source impinges on a specimen, electrons can make it through the specimen if it is thinner than ~100nm. Using different apertures, bright field, dark field, and diffraction images can be obtained from these transmitted electrons. In all these variations, one thing is common: the number and distribution of emerging electrons is turned by a computer program into an image. See, for example, Dieter K. Schroder, Semiconductor Material and Device Characterization, 2nd ed., John Wiley & Sons, Inc.

## Slide 12: Size, Shape, and Structure Observations using a TEM
Here a silver nanowire is seen at various levels of magnification and finally, on the right, at a magnification that resolves the individual atoms (The Ag atoms appear as the white “dots”)
Copyright April 2009 The Pennsylvania State University
© 2005 College of Engineering at The University of Texas at Austin. Nanoscale Materials: Metal Nanowires
Notes: <number>
The white line on the lower left of the right-hand side picture shows how wide 2 nm is. This beautiful, repetitive pattern of atoms is the signature of a crystalline solid.
Pictures like these are called micrographs.

## Slide 13: Using the Backscattered and Secondary Electrons to “See”
Seeing by using the backscattered and secondary electrons is called scanning electron microscopy (SEM). It is called field emission scanning electron microscopy (FE-SEM) when the impinging beam of electrons is produced by quantum mechanical tunneling.
Copyright April 2009 The Pennsylvania State University
Notes: <number>

## Slide 14: Schematic of a SEM or FE-SEM
Leica Leo 1530
Semiconductor Material and Device Characterization, 3rd ed.
Dieter K. Schroder, John Wiley & Sons, Inc. p 632.
Copyright April 2009 The Pennsylvania State University
Notes: <number>

## Slide 15: SEM Operation
Click on the image to view the movie
Copyright April 2009 The Pennsylvania State University
SEM Images and Text Courtesy of the Museum of Science, Boston
Notes: <number>

## Slide 16: A Size and Shape Observation using an SEM
A carbon nanotube
Copyright April 2009 The Pennsylvania State University
Copyright 2006-2009 JEOL Ltd.
Notes: <number>
The white line at the bottom of this SEM picture (micrograph) shows how wide 100nm is in this picture.
A demonstration of using an SEM for seeing can be set-up using our web based capabilities. Contact us.

## Slide 17: Outline
What do we mean by “seeing” at the nano-scale
Electron beam-based tools for producing images using electrons
Electron beam-based tools for producing composition information using x-ray photons
Scanning probe tools
How small can we go?
Key Ideas
Copyright April 2009 The Pennsylvania State University

## Slide 18: Using the X-rays to “See”
Seeing the elemental composition of a specimen by using the X-rays produced by electron impingement is called X-ray spectroscopy.
Using this technique is an example of determining chemical composition.
Copyright April 2009 The Pennsylvania State University
Notes: <number>
Composition here refers to the elemental composition

## Slide 19: An X-ray Detector Instrument
This is the X-ray detector needed. It is installed in electron microscope (TEM or SEM)
Using the detection of X-ray photons produced from the specimen as a result of electron impingement, this instrument provides spatial maps of the elements present in the regions impacted by the electron beam.
Elemental mapping can be superimposed onto the electron microscopic images and quantitative elemental information (how much of a specific element is present) can be obtained from selected spots in the images.
Courtesy of Oxford Instruments
Copyright April 2009 The Pennsylvania State University
Notes: <number>

## Slide 20: A Size, Shape, and Composition Observations using X-rays
Imaging Technology Group, Beckman Institute of Advanced Science and Technology, University of Illinois
Ni
Colors assigned to different elements
C
Ca
Na
SEM Image of a grain of sand showing well
defined regions
Composition mapping (of the regions seen in the SEM
micrograph) using X-rays
Copyright April 2009 The Pennsylvania State University
Notes: <number>
A demonstration using the x-rays produced by an SEM to map elemental composition can be set-up using our web access capability. Contact us.

## Slide 21: Outline
What do we mean by “seeing” at the nano-scale
Electron beam-based tools for producing images using electrons
Electron beam-based tools for producing composition information using x-ray photons
Scanning probe tools
How small can we go?
Key Ideas
Copyright April 2009 The Pennsylvania State University

## Slide 22: Scanning Probe Tools for Seeing at the Nano-scale
Another way to see things at the nano-scale is to use nano-scale probes. These probe-based tools can be used to let us see size, shape, structure, composition, physical properties, and chemical properties. They are generally called scanning probe microscopy (SPM) tools---scanning is in their name because they go back and forth (raster) across a surface to collect the image place by place and microscopy is in their name because they allow “seeing”.
Copyright April 2009 The Pennsylvania State University
Notes: <number>

## Slide 23: SPM Tools All Use a Probe with a Nano-scale Sized Tip
tip
sample
Copyright April 2009 The Pennsylvania State University
Image courtesy: Greg McCarty

## Slide 24: Some of the Types of Scanning Probe Tools
Atomic Force Microscope (AFM)—uses forces between atoms of the probe and those of the surface being scanned to create an image. Can be used on any surface.
Scanning Tunneling Microscope (STM)—uses quantum mechanical tunneling current between atoms of the probe and those of the surface being scanned to create an image. Can only be used on surfaces able to conduct an electric current.
Copyright April 2009 The Pennsylvania State University

## Slide 25: Some of the Types of Scanning Probe Tools (continued)
Nano-indenter—uses forces between atoms of the probe and those of the surface to determine hardness.
Copyright April 2009 The Pennsylvania State University

## Slide 26: Atomic Force Microscopes
As noted, this type of SPM uses the force between a nano-scale probe tip and the atoms of the specimen surface to create an image of the surface showing size and shape.
It is like reading Braille at the nanoscale—in this case, tactile information is converted into an image by a computer.
Copyright April 2009 The Pennsylvania State University
Notes: <number>

## Slide 27
Deflection of the cantilever due to varying forces between the nano-scale tip and the atoms of the surface is picked up by changes in the laser beam reflection and converted by a computer into a picture.
Copyright April 2009 The Pennsylvania State University
Notes: <number>

## Slide 28: An AFM Can Be Used to Produce a Picture of a Surface in Different Ways
NSF Workshop on Future Directions in Nano-Scale Systems, Dynamics and Control Metin Sitti, NanoRobotics Laboratory Department of Mechanical Engineering and the Robotics Institute Carnegie Mellon University, Pittsburgh, PA 15213-3890
In the example here, we see two of these ways: (1) following the up and down motion of the probe as it goes over a surface can be used by a computer to create a topological image of the surface or (2) the lateral deflection of the probe as it goes over the surface can be used to create a friction image. The latter also gives surface friction information.
Copyright April 2009 The Pennsylvania State University

## Slide 29: Schematic of an AFM
Image Courtesy of Veeco Instruments Inc.
Veeco Dimension 3100
Copyright April 2009 The Pennsylvania State University
© Department of Chemistry. State University of New York at Binghamton
Notes: <number>

## Slide 30: AFM Operation
Movie courtesy of Veeco Instruments Inc.
Tapping mode
Click on the black box to view the movie
Copyright April 2009 The Pennsylvania State University
Notes: <number>

## Slide 31: Size and Shape Observations using an AFM
Seeing DNA using an AFM
Copyright April 2009 The Pennsylvania State University
Courtesy of SPMage. http://www.icmm.csic.es/spmage/ "Toroidally supercoiled DNA” Dr. Jozef Adamcik. Ecole Polytechnique Federale de Lausanne (EPFL).Switzerland
Notes: <number>

## Slide 32: AFM Probes can be used to move Nano-particles
Copyright April 2009 The Pennsylvania State University
Courtesy of CNEU

## Slide 33: Scanning Tunneling Microscopes
As noted earlier, this type of SPM uses the tunneling current between the tip and the atoms of a surface to create an image and even composition information. The tunneling current is feed to a computer which turns its strength into an image position by position.
Tunneling current is a quantum mechanical phenomenon which depends extremely strongly on the distance between the tip and the type of atoms on the surface so STMs give excellent spatial resolution.
Copyright April 2009 The Pennsylvania State University
Notes: <number>

## Slide 34: Picture of the Atoms on a Silicon Surface Imaged using STM
Atoms on a silicon
surface. Note that
you can see that
Nature has made
some mistakes and
there are defect sites
where atoms are
missing.
Scanning tunneling microscopes allow surfaces to be imaged at the atomic-scale
Schematic of the scanning tunneling microscope
Image courtesy: Greg McCarty
Copyright April 2009 The Pennsylvania State University
Notes: <number>
Thermal energy gives atoms energy and the move and vibrate. At the nanoscale, all this motion is equivalent to massive earthquakes and an atom is not able to stand still at (or anywhere near) room temperature to have its picture taken. In the case the 48 iron atoms defining the quantum corral, it was necessary for Donald Eigler and his co-workers at the IBM Almaden Research Center in California to reduce the temperature within their scanning tunnelling microscope (STM) chamber to just 4 Kelvin to get the atomic motion to an acceptable level.

## Slide 35: STM Probes can also be used to move Individual Atoms or Molecules Using Voltages applied between the Tip and the selected Atom or Molecule
Copyright April 2009 The Pennsylvania State University
Courtesy of CNEU

## Slide 36: STM MANIPULATION
To move atoms and molecules, the STM tip is moved close enough to the surface adsorbate (the atom or molecule) that the tip-adsorbate attraction is comparable to the surface-adsorbate attraction. In this regime, the atom or molecule can be made to follow the tip wherever it is moved along the surface. One can then retract the tip, without causing the atom or molecule to desorb from the surface
Schematic diagram of atom or molecule
manipulation with the STM
tip
Adsorbate (atom or molecule)
Copyright April 2009 The Pennsylvania State University
© Crommie Group 2007
Notes: <number>
The next viewgraph gives a sequence of STM images showing STM manipulation of atoms to form a “corral”.

## Slide 37: Here atoms on a surface are being arranged by an STM to form a corral
Don Eigler and co-workers at IBM published these greyscale STM images showing the moving of atoms across a surface to form a corral as the corral was being constructed. The atoms were moved by the STM also by applying voltages to the probe that attracted the atom during the moving process. The atoms that form the surface itself can be seen in these STM images lying below those atoms in the process of being moved.
Some Corral Atoms
are in Position
Atoms in various
Stages of Being
Moved
Atoms of
the Underlying
Surface
Finished Corral
Copyright April 2009 The Pennsylvania State University
Science 1993
Notes: <number>
An STM was used to both move the atoms (using the forces created by the application of voltages) and image the surface.

## Slide 38: A Quantum Corral As Seen By STM
The STM tunneling current has been turned by a computer into this false color STM image
of the Quantum Corral. The computer also tilted the image for us.
Copyright April 2009 The Pennsylvania State University
Science 1993
Notes: <number>
This is a false color version of the image seen in the lower right of the previous viewgraph. The computer also titled the image for us to give some perspective. The blue things that look like “Hershey`s Kisses” are the atoms. Of course, atoms are blue and aren`t shaped like “Hershey`s Kisses”. That shape is an artifact of tunneling. The color blue was the computer programer`s choice. The red wave (color choice due to programmer) seen is the distribution of the corral atoms` electrons that have been penned-up in the “Corral”. This structure is called a quantum corral because the “red” wave seen is the quantum mechanical probability density for these electrons as predicted by Shcroedinger`s Wave Equation of quantum mechanics. As is clear, this probability density can actually be seen!

## Slide 39: Nano-Indentation Tools
Another example of a probe-based technique is Nano-indentation. This technique presses a nano-scale tip into a specimen surface at a specified rate and with a specified force thereby determining hardness.
This is an example of determining a physical property with nano-scale resolution.
Copyright April 2009 The Pennsylvania State University
Notes: <number>

## Slide 40: Nano-Indentation Operation
Scan surface of a specimen
performing indentations using selected indentation parameters (rate and force).
At each indentation, a diamond cantilever tip is lowered and forced into the target surface causing the cantilever to deflect.
By then knowing how far the tip is able to press into the surface for the specified rate and force, the material hardness can be determined.
Imaging can then be done to determine location of test.
Indentations of two different diamond-like carbon films using three different forces (23,34, and 45uN)
Image courtesy of Veeco Instruments Inc.
typical indentation tip
Copyright April 2009 The Pennsylvania State University
Image courtesy of Veeco Instruments Inc.
Notes: <number>

## Slide 41: Outline
What do we mean by “seeing” at the nano-scale
Electron beam-based tools for producing images using electrons
Electron beam-based tools for producing composition information using x-ray photons
Scanning probe tools
How small can we go?
Key Ideas
Copyright April 2009 The Pennsylvania State University

## Slide 42: So how small can we go and still “see”?
The range of some often-used characterization techniques--
Transmission Electron Microscopy (TEM)
Scanning Electron Microscopy (SEM)
Field Emission Scanning Electron Microscopy (FE-SEM)
Probe Techniques
Atomic Force Microscopy (AFM)
Scanning Tunneling Microscopy (STM))
Courtesy of Evans Analytical Group®
Note: 10 Angstoms equals 1 nanometer.
Copyright April 2009 The Pennsylvania State University
Notes: <number>

## Slide 43: Outline
What do we mean by “seeing” at the nano-scale
Electron beam-based tools for producing images using electrons
Electron beam-based tools for producing composition information using x-ray photons
Scanning probe tools
How small can we go?
Key Ideas
Copyright April 2009 The Pennsylvania State University

## Slide 44
Key Ideas
Nano-scale probes or beams of electrons, ions, or photons (light) can be used as our means to see at the nano-scale.
Signals generated by the interaction of these probes or beams with a material can be computer processed into pictures we can see.
These pictures can give us size, shape, structure, chemical and physical property information, and composition.
Copyright April 2009 The Pennsylvania State University
Notes: <number>

## Slide 45
This module, produced by the Center for Nanotechnology Education and Utilization at
The Pennsylvania State University,
is one of a series developed to introduce nanotechnology and its applications to a broad audience. Each module, its component viewgraphs, and the companion glossary are copyrighted 2009 by
The Pennsylvania State University.
All rights reserved.
Copyright April 2009 The Pennsylvania State University