## Slide 1
Introduction to Nanotechnology
Module #7
How Do You Build Things So Small:
Top-Down Nanofabrication
Nanotechnology is Impacting Everything
Copyright April 2009 The Pennsylvania State University
© patton brothers illustration (www.pattonbros.com
Last Updated: 1/6/2011
Notes: <number>
The instructor may want to break this module into two lectures. There’s a lot of material here. There is a glossary that comes along with this set of modules. Each term in blue print in every module is defined in this glossary.

## Slide 2
  This module is one of a series designed to be used by faculty members at post-secondary institutions in workshops, courses, and overview lectures to introduce nanotechnology and its applications. There is no particular significance to the module number system
  The series was funded in part by:
  The National Science Foundation
  Grant # DUE 0532646 and DUE 0802498
  and
  The Pennsylvania Department of Community and Economic Development
  Grant # C000029471 and C000036659
  Any opinions, findings, and conclusions or recommendations expressed in this material are those of the author and do not necessarily reflect the views of the National Science Foundation or the Pennsylvania Department of Community and Economic Development
Copyright April 2009 The Pennsylvania State University

## Slide 3: Glossary of Terms
Throughout these modules you will find words and terms printed in the color blue. These words and terms are defined in the glossary (glossary.html), which can be opened by clicking here.
Copyright April 2009 The Pennsylvania State University

## Slide 4: Outline
The basic approach of top-down nanofabrication
The basic steps
Deposition (or film growth)
Pattern transfer (lithography)
Etching
Materials modification
Summary
Key Ideas
Copyright April 2009 The Pennsylvania State University
Notes: <number>
The instructor may want to break this module into two lectures. There`s a lot of material here.

## Slide 5: Outline
The basic approach of top-down nanofabrication
The basic steps
Deposition (or film growth)
Pattern transfer (lithography)
Etching
Materials modification
Summary
Key Ideas
Copyright April 2009 The Pennsylvania State University
Notes: <number>
The instructor may want to break this module into two lectures. There`s a lot of material here.

## Slide 6: Top-down Nanofabrication is like Sculpting
Start with a material supported
on a substrate (or just start with
the substrate)
Add some new material
according to a pattern
(lithography; i.e., pattern transfer)
Copyright April 2009 The Pennsylvania State University
Image courtesy of Bruce Hirst
Image courtesy of Bruce Hirst

## Slide 7: Top-down Nanofabrication is like Sculpting
Subtract some of the material according to a pattern (Process order is not important; can
subtract before or after adding)
Repeat the adding/subtracting
as needed following the pattern
Copyright April 2009 The Pennsylvania State University
Image courtesy of Bruce Hirst
Image courtesy of Bruce Hirst
Notes: <number>
Following this sculpting analogy, the modification step could be coloring the eyes blue.

## Slide 8: Outline
The basic approach of top-down nanofabrication
The basic steps
Deposition (or film growth)
Pattern transfer (lithography)
Etching
Materials modification
Summary
Key Ideas
Copyright April 2009 The Pennsylvania State University
Notes: <number>
The instructor may want to break this module into two lectures. There`s a lot of material here.

## Slide 9
The building blocks of top-down nanofabrication are layers (e.g., films) of materials. These are turned into nano-structures using the basic steps of—
(1) deposition (the additive process)
(2) etching (the subtractive process)
(3) materials modification (to tailor electrical
chemical, or physical properties)
(4) lithography (providing the pattern)
Copyright April 2009 The Pennsylvania State University
Notes: <number>

## Slide 10
Etching
Lithography
Depositing
or
Growing
Material
Modification
The Basic Steps of Top-down nanofabrication.
These are used in any sequence.
Copyright April 2009 The Pennsylvania State University
Courtesy of CNEU

## Slide 11: An Example of a Top-Down Nanofabrication Processing Sequence
Copyright April 2009 The Pennsylvania State University
Film Grown by Chemical Reaction of Ambient species with the Substrate
Thin Film
Substrate
Photoresist
Mask
PLASMA ETCH
+
IONS
+
IONS
+
IONS
LITHOGRAPHY
ETCHING
Chemistry
Chemistry
Chemistry
Spin on Photoresist
Align Photomask
Expose with Light
Chemical Bonds are Altered in Exposed Areas
Dissolve Exposed Photoresist in Liquid Developer
Remove the Photoresist (Etch/Ion Implantation) Barrier
(Negative Bias)
Pattern Transfer and Substrate Modification Complete
HEAT
Substrate
THIN FILM GROWTH OR DEPOSITION
Oxygen
SURFACE MODIFICATION
+
+
+
+
+
+
+
Ion Implantation
Thermal Anneal
HEAT
Notes: <number>

## Slide 12: In the preceding cartoon sequence, all 4 steps were used. Sometimes, one or more of these steps is not needed and is omitted in nanofabrication.
Copyright April 2009 The Pennsylvania State University
Notes: <number>

## Slide 13: To summarize —
Top-down nanofabrication has four steps which are use in some sequence.
The sequence may be repeated multiple times
Steps may be skipped.
The sequence usually starts with growth or deposition of material.
Lithography is the step which orchestrates all the others. It controls where materials stay and where they are “sculpted” (i.e., etched) away.
Copyright April 2009 The Pennsylvania State University
Notes: <number>
There are hundreds of such steps used in the manufacture of a state-of-the-art chip.

## Slide 14: Outline
The basic approach of top-down nanofabrication
The basic steps
Deposition (or film growth)
Pattern transfer (lithography)
Etching
Materials modification
Summary
Key Ideas
Copyright April 2009 The Pennsylvania State University
Notes: <number>
The instructor may want to break this module into two lectures. There`s a lot of material here.

## Slide 15: Film Deposition or Growth —
Let’s look at each of these steps in more detail.
Let’s start with deposition or growth
Copyright April 2009 The Pennsylvania State University
Notes: <number>
There are hundreds of such steps used in the manufacture of a state-of-the-art chip.

## Slide 16
Material
modification
Deposition or
growth of
films/layers
Lithography
(pattern transfer)
Etching
(material
removal)
The Top-down nanofabrication methodology
Deposition or Growth Step
Copyright April 2009 The Pennsylvania State University
Courtesy of CNEU

## Slide 17
Material Growth or Deposition is needed in fabrication processing to create the basic building blocks (layers) of top-down nanofabrication.
Common processes for producing these layers include—
Growth by chemical reaction (e.g., oxidation)
Physical application (e.g., spinning layers onto a substrate)
Physical vapor deposition
Chemical vapor deposition
Copyright April 2009 The Pennsylvania State University

## Slide 18: Growth by Chemical Reaction
Thin Film
Substrate
HEAT
Substrate
(This Example Shows Oxidation)
Film Grown by Chemical Reaction of Ambient species with the Substrate
Oxygen
Copyright April 2009 The Pennsylvania State University
Courtesy of CNEU
Notes: <number>

## Slide 19
Growth by chemical reaction differs from physical application, physical vapor deposition, and chemical vapor deposition in that part of the layer is used up (chemically reacted) in any growth process.
Copyright April 2009 The Pennsylvania State University

## Slide 20: Physical Application There are many types of physical application processes; e.g., dipping, spraying, and spin-on. Here we see layer spin-on in cartoon form.
Thin Film
Substrate
Layer
Substrate
Copyright April 2009 The Pennsylvania State University
Courtesy of CNEU
Notes: <number>

## Slide 21: Physical Vapor Deposition (PVD)
In this example of PVD called sputtering, a film (purple) is being deposited
on the substrate by argon ions (green). These ions act as hammers
knocking film atoms (yellow) off the target (yellow too). A negative voltage
attracts the Ar ions to the target.
Copyright April 2009 The Pennsylvania State University
Courtesy of CNEU
Notes: <number>

## Slide 22: Chemical Vapor Deposition (CVD)
Ω
~
Impedance Match
AC Power Source
Throttle Valve
Silane
Plasma
Si
Amorphous silicon film growing
H
Gas Inlet #1
Gas Inlet #2
In this example of CVD, gas molecules (the precursor) are broken
apart by a plasma. The radicals, ions, and electrons produced result
in a chemical reaction on the substrate producing the creation of a film
as shown .
Copyright April 2009 The Pennsylvania State University
Courtesy of CNEU
Notes: <number>

## Slide 23: Outline
The basic approach of top-down nanofabrication
The basic steps
Deposition (or film growth)
Pattern transfer (lithography)
Etching
Materials modification
Summary
Key Ideas
Copyright April 2009 The Pennsylvania State University
Notes: <number>
The instructor may want to break this module into two lectures. There`s a lot of material here.

## Slide 24
Material
modification
Deposition or
growth of
films/layers
Lithography
(pattern transfer)
Etching
(material
removal)
The top-down nanofabrication methodology
Lithography
(pattern transfer)
Lithography Step
Copyright April 2009 The Pennsylvania State University
Courtesy of CNEU

## Slide 25
In top-down nanofabrication, a pattern is needed to direct where material remains and where it is removed. This pattern must be transferred (written) to where the fabrication will be done (transferred
to a substrate)
Transferring this pattern to where
it is needed (the substrate) is called “lithography”
Copyright April 2009 The Pennsylvania State University

## Slide 26: The name “Lithography” for the Pattern Transfer step comes from two Greek words:
Litho – “ stone”
Graphy– “write”
Copyright April 2009 The Pennsylvania State University

## Slide 27
The controlling pattern that is “written” to guide the fabrication processes permanently resides in a “mask”, in a mold, or in an computer data file, depending on the type of lithography.
A mask is a plate of transparent material (e.g., glass) on which a pattern resides.
A mold is a plate in which a pattern resides
Copyright April 2009 The Pennsylvania State University

## Slide 28
Basic Terms used in Lithography
Lithography – The transferring (writing) of a pattern-usually to a “resist”
Resist – Medium into which pattern on a mask, on a mold, or in computer file is transferred. Used in most types of lithography
Developer – Needed in some types of lithography to bring out the pattern written in the resist
Copyright April 2009 The Pennsylvania State University
Notes: <number>

## Slide 29
Type of Lithography | Initial Location of Pattern | “Pencil” Doing the Writing | Resist Used? | Developer Used?
Photo-lithography | Mask | Flood of light (photons) | Yes | Yes
Electron Beam Lithography | Data File | Beam of Electrons | Yes | Yes
Ion Beam Lithography | Data File | Beam of Ions | Yes | Yes
Dip Pen Lithography | Data File | Physical Contact | No | No
Embossing Lithography | Mold | Physical Contact | Yes, usually | If resist used
Flash | Mold | Physical Contact | Yes | etching
Stamp Lithography | Mold | Physical Contact | Can be | If resist used
Molding Lithography | Mold | Deposited Material | Can be | If resist used
Self-Assembly Lithography | Mask, Mold, or Data File | Deposited Material | Can be | If resist used
There are many types of lithography
Copyright April 2009 The Pennsylvania State University

## Slide 30: Most Prevalent Lithography Techniques are -
Photolithography
and
E-beam lithography
Copyright April 2009 The Pennsylvania State University

## Slide 31
Photo (or Optical) Lithography
Copyright April 2009 The Pennsylvania State University

## Slide 32: Photo (or Optical) Lithography
Mask
(pattern is on the mask)
Resist
Substrate
Visible or
UV light
Resist, which has been coated
onto the substrate, is exposed to
light—but only in regions allowed
by the mask
Copyright April 2009 The Pennsylvania State University
Courtesy of CNEU
Notes: <number>

## Slide 33: Photo Lithography (continued)
Exposed photo-resist has been designed to have its chemical bonding
changed in the regions exposed to light
Copyright April 2009 The Pennsylvania State University
Courtesy of CNEU
Notes: <number>

## Slide 34: Photo Lithography (continued)
These changed regions are then chemically attacked
by a developer and removed.
Copyright April 2009 The Pennsylvania State University
Courtesy of CNEU
Notes: <number>
Materials for which the bonding is weakened where light impinges are called a positive resist. There is also negative resists for which the bonding gets stronger where light hits. The developer for these resists removes regions where light did not impinge.

## Slide 35: Photo Lithography (continued)
The result of the chemical attack by the developer is that
the pattern is now “written” in the resist
Copyright April 2009 The Pennsylvania State University
Courtesy of CNEU
Notes: <number>

## Slide 36
The patterned resist can now be used as a chemical attack barrier (a mask*) which only allows regions with no resist covering to be chemically attacked in an etching step.
Etching then transfers the pattern to the material below and then, when this is completed, the resist is removed.
* We have to be aware of the jargon used in nanofabrication. Here the word “mask” is being used to mean a protection layer (barrier) against etching. It protects (masks) what’s below it from being subjected to chemical attack.
Copyright April 2009 The Pennsylvania State University

## Slide 37: Photo Lithography (continued)
The pattern is put into the substrate by using the resist
as a chemical-attack barrier and etching the substrate. After etching, the resist is removed and the pattern is now in the substrate.
Copyright April 2009 The Pennsylvania State University
Courtesy of CNEU
Notes: <number>

## Slide 38
Dip Pen Lithography
Another Example of a Type
of Lithography
Copyright April 2009 The Pennsylvania State University

## Slide 39: Dip Pen Nanolithography
-An AFM probe tip is used to write alkanethiols (a type of molecule) onto a surface
-Writes sub – 100 nm features
- Moving the probe tip can be slow. Manufacturing through-put problem?
S. Hong and C.A. Mirkin,
Northwestern University Center for Nanofabrication and Molecular Assembly
Copyright April 2009 The Pennsylvania State University

## Slide 40
Embossing (or Nano-imprinting) Lithography
Another Example of a Type
of Lithography
Copyright April 2009 The Pennsylvania State University

## Slide 41
Copyright April 2009 The Pennsylvania State University
Courtesy of CNEU
Notes: <number>

## Slide 42
Copyright April 2009 The Pennsylvania State University
Courtesy of CNEU
Notes: <number>

## Slide 43
Structures Produced using Patterns Created by Embossing Lithography Followed by Etching
Copyright April 2009 The Pennsylvania State University
"Current Status of Nanonex Nanoimprint Solutions," Hua Tan, Linshu Kong, Mingtao Li, Colby Steer and Larry Koecher, SPIE, (2004)
"Four-inch Photo-Curable Nanoimprint Lithography Using NX-2000 Nanoimprint," Mingtao Li, Hua Tan, Linshu Kong, and Larry Koecher, SPIE, (2004)
Notes: <number>

## Slide 44
Another example of a type of lithography
Stamping (or Soft) Lithography
Copyright April 2009 The Pennsylvania State University

## Slide 45: Stamping Lithography (also called micro-contact printing)
Think of this cartoon but with everything down at the nano-scale (no fingers!)
Uses a fabricated stamp to transfer an “ink” to form a pattern on a surface. In nanofabrication, the ink is usually molecules. What is transferred is usually a single layer of molecules.
Copyright April 2009 The Pennsylvania State University

## Slide 46
A comparison of the pattern transfer process for (1) photo- or optical,
(2) soft or stamping, and (3) embossing or nanoimprint lithography technologies.
Exploring the World of Nanoimprint & Soft Lithography-
Presented by Dr. Muhannad Bakir on Wed 01/31/07 Nano@ Tech meeting
Copyright April 2009 The Pennsylvania State University

## Slide 47: Outline
The basic approach of top-down nanofabrication
The basic steps
Deposition (or film growth)
Pattern transfer (lithography)
Etching
Materials modification
Summary
Key Ideas
Copyright April 2009 The Pennsylvania State University
Notes: <number>
The instructor may want to break this module into two lectures. There`s a lot of material here.

## Slide 48
Material
modification
Deposition or
growth of
films/layers
Lithography
(pattern transfer)
Etching
(material
removal)
The top-down nanofabrication methodology
Etching
(material
removal)
Copyright April 2009 The Pennsylvania State University
Courtesy of CNEU
Notes: <number>

## Slide 49
Etching
Etching is a subtractive processing step using one of the following:
  Wet chemical etching
  Dry physical etching
  Dry chemical/physical etching
Copyright April 2009 The Pennsylvania State University
Notes: <number>

## Slide 50
Etching—Some Key Terms
Mask- the word “mask” is used in etching terminology to mean a protective layer (covering). Ideally a mask material is not etched at all
Etch rate-how fast material is removed (usually in nm/sec)
Selectivity-how good an etching process is at attacking one material and leaving another alone
Isotropic-etching which attacks a material equally in all directions
Anisotropic-etching which attacks a material mainly in one direction
Copyright April 2009 The Pennsylvania State University
Notes: <number>

## Slide 51
Wet Chemical Etching
  Uses wet (liquid) chemical solutions
  Etching is strictly due to chemical attack
  Usually isotropic. Equal etching in all directions
  Can be very selective, etching some things and not others
Copyright April 2009 The Pennsylvania State University
Notes: <number>

## Slide 52
Wet Chemical Etching
Etch Mask
Etch Mask
Undercutting
Etching attack is
Isotropic—equal in all
directions
Copyright April 2009 The Pennsylvania State University
Courtesy of CNEU
Notes: <number>

## Slide 53
Dry Physical Etching
  Uses plasmas (a neutral “soup” made of ions, electrons, and radicals) — Etching properties of a plasma depend on the gas or gases it is made from and the power pumped into the plasma. In dry physical etching, ion bombardment (physical etching) dominates
  Strictly physical bombardment etching
  Anisotropic — because ions move from plasma toward substrate and therefore tend to bombard normal to the overall surface
  Not very selective — Bombardment knocks everything off.
Copyright April 2009 The Pennsylvania State University
Notes: <number>

## Slide 54: Dry Physical Etching Set-up
Copyright April 2009 The Pennsylvania State University
Image Credit: Huettinger Electronic
Notes: <number>

## Slide 55
Dry Chemical + Physical Etching
  Also uses plasmas. Etching properties are tailored by adjusting relative importance of bombardment (physical) etching and chemical etching (from sources such as radicals). Adjustment done by adjusting gas composition and power into plasma
  Mixture of chemical and physical etching
  Degree of anisotropy can be adjusted
  Selectivity can be adjusted
  Very useful etching method—by far, the most prevalent. Usually referred to as reactive ion etching (RIE)
Copyright April 2009 The Pennsylvania State University
Notes: <number>

## Slide 56: Dry Chemical + Physical Etching
Plasma composition adjusted (by adjusting
gases put into the
chamber) and pressure
and power are
adjusted to mix
physical and chemical etching to obtain the
degree of anisotropy
and selectivity needed
in a particular case.
Copyright April 2009 The Pennsylvania State University
Image Credit: Huettinger Electronic
Notes: <number>

## Slide 57
The creativity allowed by RIE
Changing the gas mixture employed in the plasma is used to adjust the sidewall etch profile. Note the etch selectivity is different between the resist (mask) material and the silicon
Degree of anisotropy can be adjusted
thereby adjusting the etched region’s profile
Copyright April 2009 The Pennsylvania State University
Gas mixture leading to
more isotropic etching
Gas mixture leading to
more anisotropic etching
Courtesy of CNEU
Notes: <number>

## Slide 58
Some examples of features produced by RIE
Copyright April 2009 The Pennsylvania State University
S. Topaloglu, University of Duisburg-Essen, Germany, Solid State Electronics Department
Notes: <number>

## Slide 59: Outline
The basic approach of top-down nanofabrication
The basic steps
Deposition (or film growth)
Pattern transfer (lithography)
Etching
Materials modification
Summary
Key Ideas
Copyright April 2009 The Pennsylvania State University
Notes: <number>
The instructor may want to break this module into two lectures. There`s a lot of material here.

## Slide 60
Material
modification
Deposition or
growth of
films/layers
Lithography
(pattern transfer)
Etching
(material
removal)
The top-down nanofabrication methodology
Material
modification
Copyright April 2009 The Pennsylvania State University
Courtesy of CNEU
Notes: <number>

## Slide 61: Materials Modification
Used to tailor the chemical, mechanical, optical and electrical properties in a selected region
Copyright April 2009 The Pennsylvania State University
Notes: <number>

## Slide 62
One common way to achieve materials modification in a selected region of a host material is to shoot positive ions into the region using an ion implanter. A resist can serve as a mask allowing the ions to only enter the pre-selected region.
An anneal (exposure to high temperatures in a controlled ambient) is usually part of a materials modification step. It is used after the implantation to give the implanted atoms (now atoms because they grab the necessary electrons) thermal energy to move into compatible positions in the host material.
Copyright April 2009 The Pennsylvania State University
Notes: <number>

## Slide 63: Ion Implantation
http://www2.kanazawa-it.ac.jp/sakudo-l/beginer.htm
Copyright April 2009 The Pennsylvania State University
© 2008 Spire Corporation
Notes: <number>

## Slide 64: Outline
The basic approach of top-down nanofabrication
The basic steps
Deposition (or film growth)
Pattern transfer (lithography)
Etching
Materials modification
Summary
Key Ideas
Copyright April 2009 The Pennsylvania State University
Notes: <number>
The instructor may want to break this module into two lectures. There`s a lot of material here.

## Slide 65
Now let’s re-run our example sequence where all four steps are put together to create pockets down in a substrate.
These pockets have modified properties (modified chemical, mechanical, optical, or electrical properties, as desired) designed for some use by the person who created the process sequence.
Perhaps they are designed, with further repetitions of the processing sequence, to become part of a transistor or perhaps to be regions for trapping antibodies.
The answer of what these are to become lies in the mind and in the creativity of the person who designed the lithography masks and the whole process sequencing.
We just completed looking in depth at
the four basic processes used in
top-down nanofabrication.
Copyright April 2009 The Pennsylvania State University
Notes: <number>

## Slide 66: An Example of a Top-Down Nanofabrication Processing Sequence
Copyright April 2009 The Pennsylvania State University
Film Grown by Chemical Reaction of Ambient species with the Substrate
Thin Film
Substrate
Photoresist
Mask
PLASMA ETCH
+
IONS
+
IONS
+
IONS
LITHOGRAPHY
ETCHING
Chemistry
Chemistry
Chemistry
Spin on Photoresist
Align Photomask
Expose with Light
Chemical Bonds are Altered in Exposed Areas
Dissolve Exposed Photoresist in Liquid Developer
Remove the Photoresist (Etch/Ion Implantation) Barrier
(Negative Bias)
Pattern Transfer and Substrate Modification Complete
HEAT
Substrate
THIN FILM GROWTH OR DEPOSITION
Oxygen
SURFACE MODIFICATION
+
+
+
+
+
+
+
Ion Implantation
Thermal Anneal
HEAT
Notes: <number>

## Slide 67: Outline
The basic approach of top-down nanofabrication
The basic steps
Deposition (or film growth)
Pattern transfer (lithography)
Etching
Materials modification
Summary
Key Ideas
Copyright April 2009 The Pennsylvania State University
Notes: <number>
The instructor may want to break this module into two lectures. There`s a lot of material here.

## Slide 68
Key Ideas
There are two approaches to building things at the nano-scale: top-down and bottom-up nanofabrication.
These can be combined. The combination approach is termed hybrid nanofabrication.
Top-down nanofabrication grew out of the processes used by the microelectronics industry to make chips.
Top-down nanofabrication has four key steps that are used sequentially to create nano-structures. These are (1) deposition/growth, (2) lithography, (3) etching, and (4) materials modification.
Top-down nanofabrication uses these processes to form layers (films) into nano-structures.
Copyright April 2009 The Pennsylvania State University
Notes: <number>

## Slide 69
Key Ideas (continued)
This module (Module #6) focuses on two of these four process steps:
(1) etching and (2) materials modification
Module #5 focuses on the other two of these four process steps:
(1) growth/deposition of layers and (2) lithography
Copyright April 2009 The Pennsylvania State University
Notes: <number>

## Slide 70
This module, produced by the Center for Nanotechnology Education and Utilization at
The Pennsylvania State University,
is one of a series developed to introduce nanotechnology and its applications to a broad audience. Each module, its component viewgraphs, and the companion glossary are copyrighted 2009 by
The Pennsylvania State University.
All rights reserved.
Copyright April 2009 The Pennsylvania State University