## Slide 1: Modeling a Micro Pressure Sensor Activity
Modeling a Micro Pressure Sensor Activity

## Slide 2: Unit Overview
In this activity you will use basic materials to build a macro pressure sensor with a Wheatstone bridge sensing circuit (circuit right) on a flexible diaphragm.
You will test your sensor and analyze how it works.
Results simulate those found in micro pressure sensors.

## Slide 3: Objectives
Demonstrate how a change in length and cross-sectional area affects a material's resistance.
Using your pressure sensor model, demonstrate how pressure affects the resistance and output voltage of the bridge circuit.

## Slide 4: Micro Pressure Sensors
Designed to measure absolute or differential pressures.
Convert physical quantities such as air flow and liquid levels into pressure values that are measured by an electronic system.
Used in conjunction with other sensors such as temperature sensors and accelerometers for multisensing applications.
Barometric Pressure Sensors used in wind tunnels and for weather monitoring applications.
(Photo courtesy of Khalil Najafi, University of Michigan)

## Slide 5: Micro Pressure Sensor Applications
Let’s take a look at some of the applications for which micro pressure sensor are used.

## Slide 6: Micro Pressure Sensor Applications
In the automotive industry, micro pressure sensors monitor the absolute air pressure within the intake manifold of the engine or within a tire (graphic right). They have also been designed to sense tire pressure, fuel pressure, and air flow.
  What other applications are possible within the automotive industry?

## Slide 7: BioMEMS Pressure Sensors
In the biomedical field, current and developing applications for micro pressure sensors include
blood pressure sensors (see photo right),
single and multipoint catheters,
intracranial pressure sensors,
cerebrospinal fluid pressure sensors,
intraocular pressure (IOP) monitors, and
other implanted coronary pressure measurements.
MEMS – microelectromechanical systems
MEMS Blood Pressure Sensors on the head of a pin. [Photo courtesy of Lucas NovaSensor, Fremont, CA]
Notes: The photo shows three blood pressure sensors on the head of a pin. These sensors were developed by Lucas NovaSensor to measure blood pressure and provide an electrical output representative of the pressure. RF elements are incorporated into the MEMS device allowing the sensor to transmit its measurements to an external receiver.

## Slide 8: BioMEMS Pressure Sensors
Micro pressure sensors are also incorporated into
endoscopes for measuring pressure in the stomach and other organs,
infusion pumps for monitoring blockage, and
noninvasive blood pressure monitors.
Applications of micro pressure sensors within the biomedical field and other industries are numerous.

## Slide 9: Micro Pressure Sensor Operation
To understand the pressure sensor model that you will be building, you should know how it works. So – let’s take a look.
The images in the following slides are of a micro pressure sensor built at the Manufacturing Technology Training Center (MTTC) at the University of New Mexico (UNM).

## Slide 10: A Micro Pressure Sensor
Many micro pressure sensors use a Wheatstone bridge (WB) configuration (below) as the sensing circuit.
The WB circuit is mounted on a membrane or diaphragm.
Resistors in the WB are made of a piezoresistive material.

## Slide 11: A Micro Pressure Sensor
In the circuit below, gold is used for the bridge circuit.
The pressure sensor diaphragm is a thin film of material of silicon nitride.
One side of the diaphragm is sealed to provide a reference pressure. The other side is open to the environment and subject to air pressure variation.
Pressure Sensor illustrating the Wheatstone bridge and the Silicon Nitride Membrane (Diaphragm)
[Image of a pressure sensor built at the Manufacturing Technology Training Center (MTTC) at the University of New Mexico (UNM)]

## Slide 12: A Micro Pressure Sensor
As the diaphragm moves due to pressure changes, the membrane expands and stretches. The bridge resistors mounted on the membrane also expand and stretch. This expansion translates to a change of resistance in the conductive material of the bridge. As the conductive material stretches, its resistance increases.
Pressure Sensor illustrating the Wheatstone bridge and the Silicon Nitride Membrane (Diaphragm)
[Image of a pressure sensor built at the Manufacturing Technology Training Center (MTTC) at the University of New Mexico (UNM)]

## Slide 13: Resistivity
All materials have electrical resistance.
Resistance to electrical current flow is related to a material property called resistivity (ρ), and the object’s geometry - length, width, thickness.
The combination of the geometry (shape) and material property (resistivity) determines the overall electrical characteristic (resistance).

## Slide 14: Resistivity
Resistivity is constant under constant temperature and stress (e.g., pressure).
Resistivity of a material, ρ, is inversely proportional to its conductivity, σ:
As the conductive (resistive) material stretches, the length increases while the cross-sectional area decreases. This increase in length and decrease in cross-sectional area results in an increase in overall resistance.

## Slide 15: Micro Pressure Sensor Fabrication
In this activity you build a macro-size pressure sensor that is modeled after micro pressure sensor designed and built at the MTTC / UNM. To better understand the components of your pressure sensor, let’s take a look at how a micro pressure sensor is fabricated.

## Slide 16: MTTC Pressure Sensor
Process developed at the UNM MTTC/CNM
Design incorporates a Wheatstone bridge (WB) as an electronic sensing circuit
4 Resistors (2 fixed, 2 variable)
Conducting metal is gold
4 pads as leads

## Slide 17: Determining Change in Pressure
Thin film of silicon nitride is the sensing membrane or diaphragm.
WB is fabricated on the membrane and a constant voltage is applied to the bridge.
Cavity underneath the membrane is a reference pressure.
Membrane deflects when pressures on opposite sides of the membrane are different.
As the membrane deflects, resistance changes in the variable resistors of the bridge circuit.
Amount of change in resistance is correlated to the change in pressure.
Calibration curves are created using known pressure differences.
Notes: The Wheatstone Bridge is fabricated on top of the membrane. The membrane helps to form a sealed chamber of air at room temperature and atmospheric pressure (1 atm). The chamber is actually a "hole" etched into the silicon substrate then sealed by the membrane. The sealed chamber is the reference pressure. When the air pressure above the membrane changes (increases or decreases), the pressure sensor measures the change in pressure.

## Slide 18: Pressure Sensor Physical Features
Sensing Membrane
Wheatstone bridge electronic sensing circuit
Reference chamber

## Slide 19: Pressure Sensor Fabrication Process
MTTC Pressure Sensor Process uses 2 micromachining process techniques
  Surface micromachining
  Bulk micromachining
Sensing Membrane
  Deposit Silicon Nitride thin film on silicon substrate
  Surface micromachining
Wheatstone bridge electronic sensing circuit
  Define the circuit pattern - Photolithography
  Deposit metal (chrome/gold) on membrane
  Surface micromachining
Reference chamber
  Selectively etch a hole through the silicon substrate under the membrane for the reference chamber
  Bulk micromachining

## Slide 20: Silicon Nitride Deposition
A chemical vapor deposition (CVD) process is used to deposit a thin film of silicon nitride on the silicon substrate.
CVD is the most widely used deposition method.
Films deposited during CVD are a result of the chemical reaction
  between the reactive gas(es) and
  between the reactive gases and the atoms of the substrate surface.

## Slide 21: CVD Process
  Gas molecules chemically react with each other or with the substrate forming a solid thin film on the wafer surface.
  Gaseous by-products produced by the chemical reaction are removed from the chamber.
  Substrate is placed inside reactor
  Chamber pressure is set to process pressure.
  Heat is applied (to substrate or entire chamber)
  Select (reactants) gases are introduced.

## Slide 22: Wheatstone Bridge Fabrication
Fabrication of the Wheatstone bridge sensing circuit requires photolithography and metal deposition.
The MTTC process uses metal evaporation to deposit the chrome and gold layers for the sensing circuit.

## Slide 23: Photolithography – 3 Step process
  Coat - A photosensitive material (photoresist or resist) is applied to the substrate surface.
  Expose - The photoresist is exposed using a light source, such as Deep UV (ultraviolet), Near UV or x-ray.
  Develop - The exposed photoresist is dissolved with a chemical developer.
Notes: In the etch process the exposed material of the underlying layer is etched away in either a wet or dry etch process. Once the resist pattern has been transferred to the underlying layer, the resist is removed or stripped leaving the patterned material layer.
At this point another layer is deposited on top and the photolithography process is repeated with a different pattern or mask.

## Slide 24: Metal Deposition - Evaporation Process
A thin layer of chrome followed by gold is evaporated onto the wafer.
Chamber is evacuated to process pressure.
Source material is heated to its vaporization temperature.
Source molecules and atoms travel to the wafers. Vacuum allows travel with minimal collisions.
Molecules and atoms condense on all surfaces including the wafers.

## Slide 25: Bulk Micromachining
Bulk micromachining defines structures by selectively etching inside a substrate, usually by removing the “bulk” of a material.
This is a subtractive process.
Example: Cliff dwellings at Mesa Verde, Colorado, were “bulked etched” below the surface of the flat topped mesa by man and nature.
The chamber of the pressure sensor is formed in the same manner.
[Image printed with permission from Barb Lopez]
Notes: Bulk Micromachining is a selective subtractive process which usually removes the bulk of a material. The sculpturing of Mt. Rushmore and ancient Indian cliff dwellings are examples of bulk processing. Here the idea is “Take a cliff and remove everything that doesn’t look like a dwelling”

## Slide 26: Bulk Etch – Reference Chamber
Silicon in the wafer substrate is selectively removed using anisotropic chemistries.
The silicon removed is directly beneath the WB sensing circuit.
This process allows our piezoresistive pressure sensors to be manufactured in high volume.
Front side and Backside of
MTTC Pressure Sensor
[Images courtesy of MTTC/UNM]
Notes: Bulk Micromachining is a process in which monocrystalline silicon wafers are selectively etched to form three-dimensional MEMS devices. This is a subtractive process in which the silicon substrate of the wafer is selectively removed.
Bulk micromachining takes advantage of the crystalline structure of silicon by using anisotropic etch processes. Here the etchant preferentially etches the (100) plane of the silicon – the beveled edges seen represent the (111) crystal planes which etch 400 times slower than the (100) plane. The upper photo was taken from the backside of a micro pressure sensor fabrication wafer. Bulk silicon is anisotropically etched up to the silicon nitride membrane which acts as an etch stop layer.
Using this bulk micromachining method, devices such as pressure sensors and microfluidic systems are manufactured in high volume. The bottom image shows a series of fluidic chambers and channels that have been bulk etched into a substrate.
Bulk micromachined devices typically have high aspect ratios (the ratio of height to width).
Omit the following from the script.
Credit for microfluidic chambers/channels: Microfluidic channels with high aspect ratio fluidic chambers [Image courtesy of Berkeley. Ref: C. Ionescu-Zanetti, R. M. Shaw, J. Seo, Y. Jan, L. Y. Jan, and L. P. Lee (PNAS, 2005)]

## Slide 27: Bulk Micromachining - Backside
Bulk Micromachining involves deposition, photolithography and etch.
Silicon nitride film is deposited on the backside of the wafer.
Pattern for the chamber “holes” is created in the silicon nitride using photolithography.
Bulk etch (wet anisotropic etch) is used to removed the silicon from within the “holes”.
(100)
(111)
Silicon nitride
Backside of MTTC Pressure Sensor
before (top) and after (bottom) etch
Notes: Bulk Micromachining involves elements of surface micromachining. Thin films are deposited which are subsequently patterned using photolithography and then etched using dry or wet etchants. Layers of alternating structural and sacrificial layers are deposited, patterned and etched to produce complex 3D MEMS components.
To produce a bulk etched component, the process starts with a single crystal substrate on which a thin film of material that is inert to chemical etchants is deposited.
Bulk micromachined structures can be coupled with surface micromachined components such as thin membranes, valves, thin piezoresistors and cantilevers, to produce complex devices.
Here we see two types of structures: The top images show the electronic sensing circuit of a micro pressure sensor on the left and the reference chamber on the right. The sensing circuit has been patterned into a metal layer using surface micromachining. The image on the right is the backside of the pressure sensor that consists of a bulk etched chamber. You can see the sensing elements of the sensing circuit at the top of the chamber.
The bottom image is a microfluidic membrane valve with a bulk etched inlet and surface micromachined valve plate on top and a bulk – etched silicon proof mass used in inertial sensors.

## Slide 28: Modeling a Micro Pressure Sensor
In the model that you build,
a balloon will be used as the membrane,
graphene (graphite) as the WB circuit, and
a sealed paint can as the reference chamber.

## Slide 29: What is Graphene?
Graphite is used to construct the WB circuit.
Graphite consists of stacks of graphene sheets.
Graphene is a material formed when carbon atoms arrange in sheets.
Graphene is a one-atom-thick planar sheet of carbon atoms densely packed in a honeycomb crystal lattice (as shown in the graphic right).
Notes: If you consider that the overall mass of the resistor (the total amount of the material) does not change due to the conservation of mass principal, and that the density of the material doesn’t change either, you can therefore assume that the total volume of the resistor has to stay constant. Since volume, V, can be written as a product of length (L) and area (A),
V = L x A
then as L gets longer, A must get smaller in order for the volume to remain constant.
NOTE: We have assumed the density of the material does not change; however, it could, if the temperature of the material changes. Therefore it is critical for the bridge circuit design to automatically compensate for temperature fluctuations (which could occur in a wide variety of applications).

## Slide 30: What is Graphene?
Graphene is used as the structural element for fullerenes such as carbon nanotubes (graphic) and buckyballs.
In this activity, the mixture of graphite (pencil lead) and rubber cement used to construct the WB contains sheets of graphene.
These sheets are thought to maintain contact as they slide on top of each other when the conductive material stretches.
The material stretches as pressure is applied to the membrane.

## Slide 31: Summary
Now you know how micro pressure sensors are used and fabricated.
Think about the micro fabrication processes as you construct your model.
Once your model is built, you will test it by applying various pressures and observing changes in resistance and voltage.

## Slide 32: Acknowledgements
Made possible through grants from the National Science Foundation Department of Undergraduate Education #0830384, 0902411, and 1205138.
Any opinions, findings and conclusions or recommendations expressed in this material are those of the authors and creators, and do not necessarily reflect the views of the National Science Foundation.
Southwest Center for Microsystems Education (SCME) NSF ATE Center
© 2012 Regents of the University of New Mexico
Content is protected by the CC Attribution Non-Commercial Share Alike license.
Website: www.scme-nm.org
Revised Feb 2017