## Slide 1: Photolithography overview for Microsystems
Photolithography Overview Learning Module
Patterned Mask for
Photolithography Expose

## Slide 2: Unit Overview
Photolithography occurs several times during the fabrication of a micro-sized device.
Micro-sized devices usually have several layers and each layer requires the photolithography step to identify the pattern for that layer.
This unit provides an overview of the Photolithography process and how patterns are created for each layer.

## Slide 3: Objectives
  Develop an outline of the photolithography process.
  Describe each step of the photolithography process.

## Slide 4: Photolithography and MEMS
Microelectromechanical system (MEMS) fabrication uses several layers to build micro-sized devices.
Layers include thin films of metal, bulk silicon or polysilicon.
This linkage assembly illustrates how each layer is a different component of the device, requiring a different pattern.
Photolithography defines and transfers a pattern to its respective layer.
MEMS Linkage Assembly
[Linkage graphic courtesy of Khalil Najafi, University of Michigan]
Notes: Microsystems fabrication uses several layers to build devices. These layers typically consist of thin films of metal, bulk silicon, silicon dioxide or nitride, or polysilicon. The graphic illustrates the layers of a MEMS linkage assembly. Each layer is a different component of that device. Each layer requires a different pattern.
Photolithography is the process step used to define and transfer a pattern to its respective layer. The photolithography process occurs several times during the fabrication of a microsystems device as layers build upon layers. The linkage assembly would require "at least" six layers. Can you see at least six layers? (Hint: In MEMS fabrication, some layers are “sacrificial layers”, meaning that they are completely removed leaving behind a void so that components can "float".)

## Slide 5: Photolithography and MEMS
This linkage assembly requires "at least" five layers.
Can you see at least five layers?
(Hint: In MEMS fabrication, some layers are removed completely leaving behind a void so that components can "float".)
MEMS Linkage Assembly
[Linkage graphic courtesy of Khalil Najafi, University of Michigan]

## Slide 6: Introduction – Photolithography Process
Photolithography transfers a pattern onto a wafer.
A light source is used to transfer an image on a mask to a substrate covered with a photosensitive material.
This same pattern is later transferred into another layer using a different process.
Notes: Photolithography is the process that defines and transfers a pattern onto a thin film layer on the wafer. In the photolithography process a light source is typically used to transfer an image from a patterned mask to a photosensitive layer (photoresist or resist) on a substrate or another thin film. This same pattern is later transferred into the substrate or thin film (layer to be etched) using a different process called etch.
For some layers, the resist pattern is used as a mask for a deposition process. In such cases, the patterned resist would identify the areas that receive the deposited material and the areas that do not. Patterned photoresist is also used as a hard mask for some etch processes. The photoresist is used to protect the areas of the film that are not to be etched.

## Slide 7: Photolithography vs. Photography
A twentieth century photographic process uses exposed film to create a patterned mask (negative). In a dark room, the negative is placed between a light source and a photosensitive paper.
  The paper has been coated with a light-sensitive emulsion.
  The paper is exposed when the light travels through the negative.
  The exposed paper is placed in a liquid developer which chemically reacts with the emulsion, transferring the negative’s image to the photographic paper. (see picture right)
Photographer/Painter: Jean-Pol Grandmont, shot and develop
(b&W) and scanner
[Courtesy of Jean-PolGrandmont]
Notes: The photolithography process is analogous to a twentieth century photographic process which uses exposed film as the patterned mask (referred to as a "negative" in photography). The exposed film is removed from a camera and developed to create the patterned mask or negative. In a dark room, the negative (patterned mask) is placed between a light source and a prepared sheet of photosensitive paper.
The paper has been coated with a light-sensitive photographic emulsion.
The paper is exposed when the light travels through the negative.
The exposed paper is placed in a liquid developer which chemically reacts with the emulsion, transferring the negative’s image to the photographic paper.

## Slide 8: Overview of Photolithography Steps
In the fabrication of MEMS, photolithography is used several times, any point in the process when a pattern needs to be defined.
This unit provides an overview of the three primary steps of the photolithography process:
  Coat
  Expose
  Develop
Notes: There are three basic steps to photolithography:
Coat - A photosensitive material (photoresist or resist) is applied to the substrate surface.
Expose - The photoresist is exposed using a light source, such as Near UV (Ultraviolet), Deep UV or X-ray.
Develop - The exposed photoresist is subsequently dissolved with a chemical developer. The type of photoresist (positive or negative) determines which part of the resist is dissolved.

## Slide 9: Pattern Transfer
Each layer of a MEMS or microsystems device has a unique pattern.
Photolithography transfers this pattern from a mask to a photosensitive layer.
Another process transfers the pattern from the photosensitive layer into an underlying layer.
After the pattern transfer, the resist is stripped (removed).
Pattern Transfer to Underlying Layer
Notes: In the construction of microsystems, photolithography is used at any point in the process where a pattern needs to be defined on a layer. This occurs several times during the fabrication of a microsystems device as layers build upon layers. Remember the linkage assembly device? Each layer required a pattern; therefore, each layer required photolithography.
Each layer within a microsystem has a unique pattern. The initial process used to transfer this pattern into a layer is photolithography. The photolithography process transfers the pattern of a mask or reticle (depending on the method of exposure) to a photosensitive layer (resist). In the construction of microsystem devices a subsequent process step, usually etch or liftoff, transfers the pattern from the photosensitive layer into an underlying layer.
After the pattern transfer, the resist is usually stripped or removed.

## Slide 10: Three Steps of Photolithography
  Coat - A photosensitive material (photoresist or resist) is applied to the substrate surface.
  Expose - The photoresist is exposed using a light source, such as Deep UV (ultraviolet), Near UV or x-ray.
  Develop - The exposed photoresist is dissolved with a chemical developer.
Notes: There are three basic steps to photolithography:
Coat - A photosensitive material (photoresist or resist) is applied to the substrate surface.
Expose - The photoresist is exposed using a light source, such as Near UV (Ultraviolet), Deep UV or X-ray.
Develop - The exposed photoresist is subsequently dissolved with a chemical developer. The type of photoresist (positive or negative) determines which part of the resist is dissolved.

## Slide 11: Coat Step: Surface Conditioning
In most applications, surface conditioning precedes the photoresist.
Reasons for conditioning the wafer’s surface:
  Presence of other molecules or particles create resist adhesion problems and resist thickness uniformity.
  Intermediates (i.e. HMDS) prepare the surface for adhesion by allowing
    an organic material (resist) to adhere to an inorganic surface (substrate)
    materials with different surface tensions to adhere to each other, by creating a hydrophobic surface for the resist to adhere to (which it likes to do).
The most commonly used intermediate is Hexamethyldisalizane (HMDS).
Notes: The first step of the Coat Process is Surface Conditioning. Surface conditioning prepares the wafer to accept the photoresist by providing a clean surface, coated with an intermediate chemical (such as HMDS or Hexamethyldisalizane) that creates a hydrophobic surface which boosts adhesion of the photoresist to the wafer’s surface. HMDS is the most commonly used intermediate chemical.
There are several reasons for conditioning the wafer’s surface:
The presence of other molecules or particles can create problems for resist adhesion and subsequent resist thickness uniformity; therefore, the wafer must be thoroughly cleaned and dried.
Intermediates such as HMDS prepare the surface for adhesion of photoresist.
Photoresist is an organic material that must interface with the substrate material which, in most cases, is inorganic. As an intermediate, HMDS allows this interface to occur.
Different surface materials can have different surface tensions or affinity for organic materials such as photoresist. Again, as an intermediate between the underlying surface and the photoresist, HMDS acts as a buffer and promotes the adhesion of photoresist to a variety surface materials.
Photoresist adheres best to a hydrophobic surface. A hydrophobic surface is defined as a surface which does not like (phobic) water (hydro). A layer of HMDS provides a hydrophobic surface.

## Slide 12: Surface Conditioning
Photoresist adheres best to a hydrophobic surface (a surface devoid of water molecules).
It is the role of HMDS to provide such a surface.
Before applying the HMDS, any water molecules present on the wafer are removed by heating the wafer to 100°C.
Hotplates are used to remove moisture from the wafer's surface or from coatings placed on the surface. When the wafer is placed on the hotplate, the pins lower to provide contact between the hotplate and the wafer.
Notes: There are three basic steps to conditioning the wafer’s surface: bake, prime and cool.
Bake
After the wafer is cleaned (rinsed/dried) and prior to applying a primer (HMDS), water molecules present on the wafer surface must be removed. One way is to heat the wafer to 100° C, the boiling point of water. The wafer is heated or baked in a small vacuum chamber or on a hot plate to remove water molecules on the wafer surface.

## Slide 13: Surface Conditioning
  Prepares the wafer to accept the photoresist by providing a clean surface.
  Heats the wafer to remove water molecules on the wafer surface.
  Coats the wafer with an intermediate that boosts adhesion of the photoresist to the wafer’s surface. (Usually Hexamethyldisalizane or HMDS)

## Slide 14: Surface Conditioning Steps
Three basic steps:
  Wafer is baked to remove the water molecules on the wafer surface
  HMDS is applied (prime) to create a hydrophobic surface
  Wafer is cooled to room temperature.
Notes: There are three basic steps to conditioning the wafer’s surface: bake, prime and cool.
Bake
After the wafer is cleaned (rinsed/dried) and prior to applying a primer (HMDS), water molecules present on the wafer surface must be removed. One way is to heat the wafer to 100° C, the boiling point of water. The wafer is heated or baked in a small vacuum chamber or on a hot plate to remove water molecules on the wafer surface.
Prime
HMDS is applied (prime) to create a hydrophobic surface. The hydrophobic surface prevents water molecules from re-accumulating on the surface once the wafer is returned to the environment.
Cool
After the wafer is primed, it is cooled to room temperature (sometimes using a chill plate). This brings the wafer to the same temperature as the resist for the subsequent resist dispense step.
After the surface is conditioned, the wafer is coated with photoresist.

## Slide 15: Photoresist (Resist)
A mixture of organic compounds in a solvent solution.
There is negative or positive photoresist (depending on how it responds to light)
Negative resist - Exposed materials harden. A negative mask is left after develop.
Positive resist - Exposed regions become more soluble. A positive mask is left after develop.
Photoresist - Positive vs. Negative
Notes: Photoresist is a mixture of organic compounds held together in a solvent solution.
There are two basic types of photoresist: negative or positive. Their primary difference is how they respond to the light source (as shown in the graphic).
Negative resist and UV: The regions of resist exposed to ultraviolet light (UV) become insoluble or harden. When developed, the hardened resist remains on the wafer and the non-exposed resist dissolves. The result is a negative resist pattern on the wafer.
Positive resist and UV: The regions of resist exposed to the UV become more soluble. When developed, the exposed resist dissolves and the unexposed resist remains. A good way to remember this is “What shows, goes”. The result is a positive resist pattern on the wafer. Positive resist is more commonly used for microsystems fabrication.

## Slide 16: Coat Process
  The coat process is the application of photoresist to the wafer’s surface.
  The resist must be
    thick enough and durable enough to withstand the next process steps and
    uniform (evenly distributed) in order to prevent problems during the expose process.
Notes: The coat process is the application of photoresist to the wafer’s surface. There are several methods used to coat the wafer (spin, spray and electrodeposition (ED)). The goal of the coat process is to distribute a uniform thickness of resist across the wafer's surface with a desired thickness. The resist must be thick enough and durable enough to withstand the next process steps. It must also be uniform in order to prevent problems during the expose process.
Spin coating is the most common methods for coating a wafer. The image below shows a spin coater. You can see the wafer sitting on the chuck and the excess resist (red) that has spun off the wafers.

## Slide 17: Spin Coating
The most common method for coating a wafer.
  Wafer is placed on a vacuum chuck
  A vacuum holds the wafer on the chuck
  Resist is applied
  Chuck accelerates for desired resist thickness
  Chuck continues to spin to dry film
Spin Coating
Notes: The wafer is placed on a vacuum chuck.
A vacuum chuck holds the wafer.
Photoresist is applied either before the chuck begins to spin (static dispense), or when the chuck starts to spin slowly (dynamic dispense).
The chuck quickly accelerates to a pre-programmed rpm to spread the resist across the entire wafer.
At maximum spin speed (SS) the excess resist is thrown off the wafer and a uniform resist thickness results.
The chuck continues to spin until most of the solvents in the resist have evaporated.

## Slide 18: Challenge Question
What could affect the uniformity of the photoresist during the coat process?

## Slide 19: Softbake
After the photoresist is applied to the desired thickness, a softbake is used to remove the residual solvents of the photoresist.
After the softbake, the wafer is cooled to room temperature.
Softbake after Applying Resist
Notes: After the photoresist is applied to the desired thickness, a softbake is used to remove the residual solvents of the photoresist.
After the softbake, the wafer is cooled to room temperature.

## Slide 20: Alignment
"Align" is one of the most critical step in the entire microsystems fabrication process.
Due to the microscopic size of these devices, a misalignment of one micron or smaller can destroy the device and all the devices on the wafer.
Each layer must be aligned properly and within specifications to the previous layers and subsequent layers.
Microscopic Hinge
[Photo courtesy of Sandia National Laboratories]
Notes: The expose process consists of the align and expose steps.
Alignment is one of the most critical steps in the entire microsystems fabrication process. Due to the microscopic size of these devices, a misalignment of one micrometer (micron or 1μm) or even smaller can destroy the entire device and all the other devices on the wafer. It is important that each layer is aligned properly and within specifications to the previous layers and subsequent layers.

## Slide 21: Misalignment
Take a look at the microscopic hinge. Notice the 1μm scale in the bottom right. Using this scale, we might estimate the width of the space between the hinged component and its enclosure (the loop) to be approximately 0.5 μm or 500 nm.
What would be the result if the mask for the loop was misaligned by 0.5 μm?
Microscopic Hinge
[Photo courtesy of Sandia National Laboratories]
Notes: Take a look at the microscopic hinge. Notice the 1μm scale in the bottom right. Using this scale we might estimate the width of the space between the hinged component and the edge of the loop to be approximately 0.5 μm or 500 nm.
What would be the result if the mask for the loop component was misaligned by 0.5 μm?

## Slide 22: Mask vs. Reticle
A patterned mask (or reticle) is a quartz or glass plate with the desired pattern (usually in chrome). The picture shows a “mask” used to expose an entire wafer.
Notice the repeating pattern throughout the mask. Each pattern is a “reticle” or pattern for one device.
Expose equipment may use a whole mask or a smaller quartz plate with just a few reticles (inset).
Mask and Reticle (inset)
Notes: The patterned mask (or reticle) is a quartz or glass plate with the desired pattern (usually in chrome). The picture shows a mask used to expose an entire wafer. Notice that there is a repeating pattern throughout the mask. Each of these patterns is a die containing few micro-sized components, in the case shown here.
Some equipment do not use masks. Instead a smaller quartz plate is used with just a few die (inset).

## Slide 23: Align
The mask or reticle is locked into the expose equipment and the wafer is aligned to the mask along the x and y coordinates.
The z-coordinate is adjusted to define the focal plane of the image.
When a mask is used, a single pulse of light expose the entire wafer.
When a reticle is used, the reticle is "stepped" around the wafer exposing a small amount of the wafer with each step.
Quartz Mask
Notes: Regardless of which is used, a mask or a reticle, the plate is locked into the expose equipment. The wafer is aligned to the mask or reticle along the x and y coordinates. The z-coordinate is adjusted to define the focal plane of the image.
When a mask is used, a single pulse of light will expose the entire wafer. When a reticle is used, the wafer or the reticle is “stepped” in the x, then y directions, exposing a small portion of the wafer with each step. This type of expose equipment is called a "stepper".

## Slide 24: Expose
The wafer is exposed by UV (ultraviolet) from a light source.
UV travels through the mask to the resist.
A chemical reaction occurs between the resist and the UV.
Only those areas not protected by the mask undergo a chemical reaction.
Notes: During expose, the photoresist layer is exposed when ultraviolet (UV) light from a source travels through the mask to the resist, exposing the resist. UV light sources normally include mercury vapor lamps and excimer lasers. The UV light hitting the resist causes a chemical reaction between the resist and the light. Only those areas not protected by the mask undergo a chemical reaction.

## Slide 25: Review Question
Remember positive vs. negative photoresist?
  What happens when UV hits negative resist?
  What happens when UV hits positive resist?
Notes: Let's see if you remember what happens when the light hits the resist. Do you remember positive vs. negative photoresist?
What happens to exposed negative resist?
What happens to exposed positive resist?

## Slide 26: Develop
A chemical developer dissolves portions of photoresist.
With positive resist, the exposed resist is dissolved while the unexposed resist remains on the wafer.
With negative resist, the unexposed resist is dissolved while the exposed resist remains.
The develop process leaves a visible pattern within the resist.
The Develop Process
Notes: In the develop process, portions of the photoresist are dissolved by a chemical developer. With positive resist (the more commonly used resist), the exposed resist is dissolved while the unexposed resist remains on the wafer. With negative resist, the unexposed resist is dissolved while the exposed resist remains.
The develop process leaves a visible pattern (seen by the naked eye) within the resist.

## Slide 27: Develop
Develop is a wet process.
Wafers are immersed in the developer or the developer is sprayed on a wafer.
Timing is critical. Too little or too much time could affect the critical dimensions of the pattern transfer.
To stop the chemical reaction of the developer with the photoresist, the wafers are rinsed with DI water then spin-dried.
Notes: Develop is usually a wet process. The wafers are physically placed in the develop solution (immersion) or the developer is sprayed onto the wafer.
The timing of this process is critical. Too long of a time leads to an "overdeveloped resist"; too little of a time leads to an "underdeveloped resist" – both of which negatively affect line width. An underdeveloped resist could prevent access to the underlying layer by leaving too much resist on the wafer.
To stop the chemical reaction of the developer with the photoresist, the wafers are rinsed with de-ionized (DI) water then spin-dried.

## Slide 28: Hardbake
Post-develop hardbake hardens the photoresist for the next process.
The temperature of the hardbake is higher than the softbake after coat. However, too high of a temperature could cause the photoresist to reflow, destroying the pattern.
After the hardbake, the wafer is cooled to room temperature.
Hardbake

## Slide 29: Inspect
Wafers are inspected immediately after the photolithography process.
Three critical parameters inspected are alignment, line widths and defects.
Alignment – Is the pattern positioned accurately to the previously layer?
Line width or critical dimension (CD) – Are pattern images in focus and have the correct size (CD)?
Defects – Are there defects that could affect subsequent processes or the operation of the device?
  e.g. particles, scratches, peeling (lifting) of the resist, holes in the resist, scumming (an underdeveloped or underexposed pattern)

## Slide 30: Inspect
High powered microscopic equipment is used to inspect wafers.
Software measures the width of a printed structure and provides information to the technician.
Alignment marks are designed into the masks and reticles and patterned into each layer as reference points during inspect. This allows the overlay of a subsequent step to be measured against the previous step to identify misalignment or CD.
Wafer Inspect
[Photo courtesy of the MTTC, University of New Mexico

## Slide 31: Let’s Think About It
What are some of the critical parameters inspected during the photolithography process and as a final inspection?
Critical dimensions are getting smaller. Objects are getting smaller. In microsystems technology, some objects are required to "float" above the substrate.
What do you think are some of the limitations, if any, of the photolithography process described here when applied to these advancing technologies?

## Slide 32: Summary
Photolithography uses three basic process steps to transfer a pattern from a mask to a wafer: coat, develop, expose.
The pattern is transferred into the wafer’s surface layer during a subsequent process.
In some cases, the resist pattern can also be used to define the pattern for a deposited thin film.

## Slide 33: Disclaimer
The information contained herein is considered to be true and accurate; however the Southwest Center for Microsystems Education (SCME) makes no guarantees concerning the authenticity of any statement. SCME accepts no liability for the content of this unit, or for the consequences of any actions taken on the basis of the information provided.

## Slide 34: Acknowledgements
Made possible through grants from the National Science Foundation Department of Undergraduate Education #0830384, 0902411, and 1205138.
Any opinions, findings and conclusions or recommendations expressed in this material are those of the authors and creators, and do not necessarily reflect the views of the National Science Foundation.
Southwest Center for Microsystems Education (SCME) NSF ATE Center
© 2010 Regents of the University of New Mexico
Content is protected by the CC Attribution Non-Commercial Share Alike license.
Website: www.scme-nm.org
March 2017