## Slide 1: MicroCantilever applications overview
Microcantilevers Learning Module

## Slide 2: Unit Overview
The microcantilever is a widely used component in MEMS (microelectromechanical systems).
Its flexibility and versatility make it a popular component for applications in a number of fields.
This unit discusses many of these applications.

## Slide 3: Objectives
Discuss four different applications in which microcantilevers are used.
Discuss the advantages and limitations of microcantilevers compared to macrocantilevers.

## Slide 4: Introduction
A cantilever is a suspended beam, supported at only one end. Aircraft wings, balconies, diving boards, and free standing radio towers are types cantilevers.
Cantilevers come in all sizes. Macrocantilevers range in length from a few meters to hundreds of meters.
Microcantilevers are a few micrometers to several hundred micrometers in length.
Types of Cantilevers

## Slide 5: Microcantilever Applications
Microcantilevers are used as sensors, transducers, probes, needles, transport mechanisms, and switches for many tasks.
  Detect physical, chemical, and biological particles
  Penetrate tissue in therapeutic and diagnostic applications
  Sensors to detect nano-size particles on a surface
  Memory storage devices
Scanning Electron Microscope (SEM) image of a Cantilever Sensor Array
These cantilevers were developed by the Swiss Nanoscience Institute for proteomic and genomic applications.
[Image courtesy of Dr. Christoph Gerber, Institute of Physics, University of Basel]

## Slide 6: Cantilever-based MEMS
Current applications of cantilever-based MEMS:
  Biomedical Applications (BioMEMS)
  pH sensors
  Therapeutics
  Atomic Force Microscopes (AFM)
  Read/Write storage devices
  Environmental Monitoring
  Food Production and Safety
  RF Switching

## Slide 7: Microcantilever Materials
Microcantilevers are fabricated from various materials, most commonly from silicon, silicon nitride (SiN), and polymers.
Application of the cantilever determines the coating or subsequent layers.
Type of material and physical dimensions are determined by the cantilever's application and operational requirements.
Cantilever Beam of silicon nitride (SiN) coated with a gold layer

## Slide 8: Application vs. Stiffness
Probes and needles need to be stiff enough to penetrate tissue without bending.
Resonators, and latches need to be stiff enough so as not to oscillate too easily or flex due to weak ambient forces.
Cantilever sensors, transducers and switches need more flexibility.
Probes with MEMS sensors at the probe tips

## Slide 9: Microcantilever Fabrication
Fabricated using both bulk and surface micromachining.
In each process, a solid structure is released from the crystal silicon to create a free-standing beam, anchored at one end.
Micromachining processes allow for the fabrication of a single cantilever or an array of cantilevers.
MEMS Cantilever Array YouTube Video
(Click on graphic to start YouTube animation.)

## Slide 10: Microcantilever Characteristics
This popularity of the microcantilever in MEMS is due several characteristics which include the following:
Ability to render measurable mechanical responses quickly and directly
Sensitivity to a miniscule amount of external force or stimuli
Low power consumption
Capability to fabricate a high density array with simultaneous responses to different stimuli – each cantilever in the array is individually functionalized.

## Slide 11: Microcantilevers as Sensors
Sensors are the most versatile applications of MEMS.
MEMS sensors can be either a micro or nano-sized device.
Their size allows them to interface with integrated circuits on the same chip in order to provide analysis and feedback.
Eight cantilevers coated with palladium-nickel films. Two reference cantilevers left uncoated) [University of California at San Diego project, headed by Michael Sailor, a professor of chemistry and biochemistry.]

## Slide 12: Sensor Coating
To sense the presence of a certain particle or analyte, microcantilevers are coated (functionalized) with a chemically sensitive material or probe coating.
The type of material can provide for a high degree of specificity in detecting certain particles or "analytes" within a sample (e.g. The Enose (electronic nose).
Probe Coating (A chemically sensitive material that absorbs select analytes in a sample)

## Slide 13: Properties of Measurement
As sensors, microcantilevers rely on their flexibility or “spring constant” to create some type of measurable change when exposed to external stimuli.
The cantilever's reaction to an external stimulus is referred to as mechanical stress. This stress results in a change in one of the cantilever's mechanical or electrical properties:
  Angular deflection
  Resistivity
  Natural resonant frequency

## Slide 14: Microcantilevers in Sensors
Microcantilevers can be fabricated as a single device (left figure) or as several devices arrange in a sensor array (right figure). Applications for cantilever-based sensor arrays are endless.
Single MEMS probe with electronics
Cantilever Array for Read/Write Memory
[Image courtesy of IBM]

## Slide 15: Chemical Sensor Arrays
A chemical sensor array (CSA) is designed to detect and measure the amount or concentration of one or more substances within a given sample or environment.
Examples:
  CSAs used in the medical field can identify the amount of a specific antibody or antibodies with a small blood sample.
  An artificial nose is a CSA used to recognize certain vapors and their concentrations.

## Slide 16: Chemical Sensor Array
CSAs are chemically discriminating. An individual cantilever or a set of cantilevers can be designed to detect one and only one analyte within the sample OR an array can have numerous discriminating cantilevers allowing for the detection of several different analytes within the same sample (see figure).

## Slide 17: Microcantilever Sensors and Sensor Arrays
  Gas leak detectors
  Detection and characterization of chemicals in liquid and gaseous states
  Biosensors (detect and measure antibodies, protein, enzymes, antigens, and DNA)
  Sensors for DNA hybridization and Protein binding
  pH sensors
  Biomolecular analysis

## Slide 18: Advantages of Microcantilever Sensors
  Microscale size
  Ease of constructing many cantilevers in one array
  Ability to detect multiple analytes in one solution using one MEMS device
  Extremely high sensitivity and selectivity
  Flexibility of its working environment (air, vacuum, liquid)
  Wide dynamic range
  Low power consumption

## Slide 19: Microcantilevers as Transport Devices
As sensors, microcantilevers need some degree of flexibility in order to "bend" when exposed to its target.
As a transport device, a microcantilever needs a higher degree of stiffness. However, for some transport applications, such as the Atomic Force Microscope cantilevers, some "bending capability" is still required.
Following are applications for cantilevers used as transport devices.

## Slide 20: Cantilevers as Surface Probes: AFM
An Atomic Force Microscope (AFM) is a high-resolution scanning probe microscope.
As the sample moves in the x-y directions, the microcantilever “senses” the surface topography.
A laser is reflected off the top of the cantilever.
The z-motion of the cantilever changes the angular deflection of the laser.
These changes are detected and translated into a 3-dimensional representation of the sample surface.
AFM Cantilever and Probe Tip

## Slide 21: Read / Write Storage
In storage devices a microcantilever transports a probe over a polymer storage medium. The probe tips have a diameter of ~ 10 nm.
To read, the tips detect the presence or absence of matter in the polymer film. To write, they move or displace matter a few nanometers in width (see figure).
It is projected that MEMS read/write storage devices will be able to store 1 Tbit/in2 (1 Gbit/mm2) of data in a unit the size of a postage stamp.
NOTE; Even though several prototypes of this device have been made, as of 2015 such devices are not commercially available. Following is a brief discussion of the IBM Millipede Prototype.
Close-up of read/write cantilevers showing displacement of matter in a polymer film. [Picture courtesy of IBM)

## Slide 22: IBM Millipede Prototype
The Millipede consists of a micro-cantilever array positioned over a polymer film storage medium.
The most recent prototype (2005) consists of a 64 x 64 array of 4,096 cantilevers.
An electromagnetic actuation precisely moves the storage medium in the x-y directions.
Each probe tip reads and writes to a storage area of 100 μm x 100 μm.
IBM Prototype (32 x 32 array)
[Picture courtesy of IBM)

## Slide 23: Millipede Videos
Millipede Close Up – Courtesy of IBM
Millipede Array – Courtesy of IBM

## Slide 24: Microcantilevers as Switches
MEMS switches are typically broadband switches (can operate over a wide frequency range).
In theory, MEMS RF (radio frequency) switches can direct and control signals as high as 50 GHz and possibly higher.
Because of their low power consumption MEMS switches significantly increase the battery life of many handheld applications such as cell phones and PDAs.

## Slide 25: A MEMS RF Switch
A MEMS RF switch is a metal microcantilever with a metal contact tip.
When a voltage is applied to the Pull-Down Electrode, the resultant electrostatic force pulls the cantilever contact towards the lower contact until the two come together.
Upon contact, the switch is closed.
MEMS RF Switch

## Slide 26: Microcantilevers as Needles
A micro-needle takes a small blood sample (picoliters) by drawing blood flow via capillary force. Because of size, the injection is relatively painless.
Micro and nano-sized needles are used singly and in needle-arrays for drug delivery applications. (image right)
These needles can be made of silicon with each needle measuring 40 μm in diameter and 500 μm tall.
Illustration of a Microneedle array and a needle’s tip that could be used as a Transdermal Drug Delivery System

## Slide 27: Microcantilevers as Probes
Diseases such as Parkinson's and Alzheimer's have helped to mobilize research into using micro and nano-sized cantilevers as neural probes (see figure).
Applications of Neural probes:
  Studying the central and peripheral nervous system
  Treating Neurological disease through the use of neural prostheses
  Studying the brain network

## Slide 28: Cochlear Implant
For the hearing impaired, a Cochlear implant is a neuroprosthetic that allows a deaf person to hear noises never heard before. (See diagram of Cochlear Implant)
Neuroprosthetic devices have become one of the most important emerging technologies in biomedical engineering applications.
Cochlear Implant
[Image courtesy of National Institute of Health]

## Slide 29: Let’s Review
What appears to be one of the major applications for microcantilevers?
What are some possible applications of microcantilevers not discussed in this presentation?
How does application determine the stiffness of the cantilever?

## Slide 30: Summary
Microcantilevers are used for many applications. The specific application determines the geometric shape of the cantilever, the material from which it is made, and its stiffness characteristics.
The microcantilever is the cornerstone component of a wide variety of MEMS including micro-chemical sensor arrays, atomic force microscopes, microswitches, and neural probes.

## Slide 31: Acknowledgements
Made possible through grants from the National Science Foundation Department of Undergraduate Education #0830384, 0902411, and 1205138.
Any opinions, findings and conclusions or recommendations expressed in this material are those of the authors and creators, and do not necessarily reflect the views of the National Science Foundation.
Southwest Center for Microsystems Education (SCME) NSF ATE Center
© 2012 Regents of the University of New Mexico
Content is protected by the CC Attribution Non-Commercial Share Alike license.
Website: www.scme-nm.org
Revised Feb 2017